Preservation Note 43

Restoring and Maintaining Terrazzo Flooring

Finishes

August-99

Stone Flooring-09400

Restoring and Maintaining Terrazzo Flooring

Terrazzo is a man-made stone composed of marble and granite chips mixed with a binder. Three types of binders are used: Portland Cement, Polyacrylic-modified Portland Cement with an acrylic additive, and epoxy or polyester resin material used in thin-set terrazzo. Terrazzo comes in a variety of colors depending on the stone used in the mixture and the tint of the cement binder. It can be poured in place or precast and is installed with dividing strips that serve as control joints. Originally these strips were wood, but are now made of white alloy of zinc, brass, or colored plastic. Like stone, terrazzo is ground to a smooth surface, polished to a shiny finish, and sealed for protection.

Terrazzo is durable and easy to maintain, and is often installed in high traffic areas such as lobbies and corridors. It is important to determine what type of terrazzo is installed before planning any maintenance or restoration work. Different types of terrazzo require different treatments. It is primarily the type of binder that dictates the proper chemicals, cleaning procedures, and restoration methods.

All terrazzo work should comply with specified provisions and recommendations of the National Terrazzo and Mosaic Association, Inc. (NTMA), 110 E. Market Street, Suite 200 A, Leesburg, Virginia 20176, (703) 779-1022 or (800) 323-9736, FAX (703) 779-1026, E-mail info@ntma.com, Web www.ntma.com.

Maintaining A Terrazzo Floor

Proper preventive and routine maintenance is required to keep a terrazzo floor in good condition.

Preventive Maintenance

Seek professional help to establish the type of terrazzo installed. This will help plan and execute appropriate maintenance procedures.

Provide floor mats or area rugs inside and outside entrances to prevent dirt, grit, acidic rain water, rock salt, ice melt, and other abrasive material from being dragged across the terrazzo floor. Be sure underside of mats and rugs have non-slip surface.

Keep floor dirt and dust free. Dirt particles can scratch the terrazzo and dust makes the floor slippery. High traffic areas should be cleaned more often. Walkways outside of entrances should be swept to prevent dirt particles from entering building.

Clean spills immediately before they stain. Keep water from spilling on the surface, especially around drinking fountains and planters.

Keep metal objects away from terrazzo. A metal can could rust and stain terrazzo if exposed to moisture.

Protect the terrazzo with a sealer to prevent absorption of dirt and stains and provide a slip resistant surface.

Sealer guidelines:

The type of sealer required depends on the type of binder used. Portland Cement systems must be sealed with a penetrating solvent-type sealer immediately after polishing to protect the porous cement binder. Resinous systems can be sealed with a non-penetrating or surface type sealer since the matrix in this system creates a non-porous surface.

Be sure finish is slip resistant.

Be sure floor surface is clean of all dirt and particles before application.

Apply sealer according to the manufacturer's instructions.

Do not use wax or general-purpose sealers. The floor could be slippery after application.

Penetrating sealers do not result in high sheen. Apply high luster finish coat on top of sealer for higher gloss.

Twice a year strip old sealer and any finish coats and reseal floor.

Routine Maintenance

Dust mop frequently, especially in high traffic areas. Dirt and grit are abrasive and scratch terrazzo floors and dust can cause a slippery surface. Sweeping compounds can be used, but avoid compounds with oil, sand, or abrasives. The oil could permanently discolor the terrazzo and the sand and abrasives could scratch the surface.

For general cleaning, use a neutral cleaning compound diluted according to the manufacturer's directions. Select a product with a pH factor between 7 and 10. Avoid washing solutions that contain alkali, acid, carbonates, trisodium phosphate, and other strong ingredients which might damage floor. Do not use all-purpose cleaners or soaps and scrubbing powders containing water-soluble, inorganic salts, or crystallizing salts. Improper cleaning materials can damage terrazzo.

Cleaning guidelines:

Always use clean water and equipment.

Floor should be pre-wet with clean, warm water before beginning the washing operation.

Mix neutral cleaner with clean water.

For heavily soiled floors increase the amount of compound.

Apply according to manufacturer's instructions.

Allow to remain on floor for several minutes to dissolve the dirt.

Keep floor wet during process so dirt does not reabsorb into floor.

Rinse well with clean water and remove solution with squeegee, wet vacuum, or mopping.

Allow to dry and buff with a dry brush.

Electric- or battery-powered scrubbing machines should be used periodically with a solution of neutral compound to loosen dirt. Floor machines should be equipped with fiber brushes, or with abrasive nylon pads.

Buffing the floor with a powered machine and an acrylic water-based finish after each cleaning restores the luster to the surface, building a natural sheen.

Promptly clean stains and scuffmarks with a neutral cleaner diluted with warm water. Steel wool should not be used on terrazzo to remove stains; it may rust and stain the surface.

Restoring A Terrazzo Floor

Over time, a terrazzo floor may need restoration work to repair any damage and restore the surface finish. Restoration of a terrazzo floor requires professional technicians and special procedures.

Refinishing Discolored or Damaged Terrazzo Floors

Older terrazzo floors may be discolored or have a damaged surface because of a build-up of old finishes or soap scum, overuse of disinfectants and coatings, or because of dirt tracked into the floor. These floors should be stripped to the original surface, cleaned, and then sealed.

Determine type of terrazzo and select appropriate products.

Always wear protective gear and work in well-ventilated area when handling any chemicals.

Test an area of each terrazzo type before stripping, cleaning, and sealing all the terrazzo.

Avoid contact of chemicals with adjacent surfaces.

Strip existing sealers and coatings from floor.

Use neutral liquid chemical cleaner with a pH factor between 7 and 10, formulated for the specific type of terrazzo.

Following manufacturer's directions, apply chemical floor cleaner and let stand recommended time or time determined by test area.

Apply a mist of water over the cleaner on the floor.

Pick up residue with a wet vacuum.

Using a power scrubber with a scrub brush attachment, fiber bristle brush, or white nylon pad, scrub the floor until all coating material has been removed.

Pick up all liquid residues with a wet vacuum.

Thoroughly rinse the surface with clean water.

Pick up all remaining liquid residues with a wet vacuum and allow floor to dry.

Do not use metal brushes or steel wool.

Repeat process if necessary.

Clean the surface using a mildly abrasive phosphate free cleaning compound containing no caustic or harsh fillers, formulated specifically for restorative type cleaning of terrazzo.

Apply new sealer using a colorless, slip and stain resistant sealer with a pH factor between 7 and 10, that does not affect the color or physical properties of the terrazzo surface.

Always use clean water and remove all liquid with a wet vacuum.

See the GSA Historic Preservation Technical Procedures titled, "Stripping And Cleaning Dirty Or Discolored Terrazzo Floors" and "Stripping Built-up Coatings From Terrazzo," found on the GSA web site at http://w3.gsa.gov/web/p/hptp.nsf?OpenDatabase, for detailed information on products, manufacturers, and procedures.

Regrinding Terrazzo Floors

If dirt, scratches, and the build-up of coatings are so severe that normal stripping and cleaning cannot restore the floor, or if the floor is heavily worn, the surface may be stripped using fine grit stones and resurfacing screens. This method involves grinding off a thin layer of the terrazzo and should only be used as an extreme measure. The work must be performed by an experienced professional.

Grind and polish the terrazzo floor to produce a clean, smooth, uniform finish.

Be careful grinding around dividing strips.

For small areas use hand sander or small grinding tool; for larger areas use a circular buffing machine with grinding and polishing pads.

Use a #24 or finer grit stone/screen (fine mesh sand may also be used) for the initial grinding, exposing the marble chips. Follow with a fine #80 or finer grit stone/screen.

Rinse floor thoroughly with clean water and remove excess rinse water.

Machine or hand-apply grout using matching Portland Cement, filling all voids completely.

Cover grouted surface with paper or polyethylene for at least 72 hours.

Final polish with a #80 or finer grit stone until grout has been removed from the terrazzo surface.

Wash surface with neutral cleaner and thoroughly rinse with clean water. Allow surface to thoroughly dry.

Seal terrazzo with a colorless, slip and stain resistant penetrating sealer with pH factor between 7 and 10, that does not affect color or physical properties of the terrazzo.

See the GSA Historic Preservation Technical Procedure titled, "Regrinding Terrazzo Floors," found on the GSA web site at http://w3.gsa.gov/web/p/hptp.nsf?OpenDatabase, for detailed information on products, manufacturers, and procedures.

Repairing Chips and Cracks in Terrazzo

GSA's Historic Preservation Technical Procedures includes guidelines for repairing chips and cracks in terrazzo using either a cement grout or epoxy resin, depending on the original binder used in the terrazzo. It is recommended that minor chips and cracks be repaired only when surface irregularities present safety hazards or when it is necessary to prevent further deterioration to the terrazzo.

Patching Minor Chips and Cracks in Terrazzo with Cement Grout

With a power saw or hand tools, cut a vertical perimeter wall around the area to be patched.

Clean the surface of debris and saturate the void with water.

Apply cement paste and work into surface. Do not allow cement paste to dry before placing terrazzo composition.

Mix terrazzo composition, matching marble chips and matrix for existing terrazzo by size, mineral content, and color.

Place mixture over chip or crack and level with a trowel.

Compact patch, removing all excess water and cement from the surface.

Cover the patch with paper or polyethylene sheeting to prevent quick hydration. Cure until topping develops sufficient strength to prevent lifting or pulling of terrazzo chips during grinding.

Sand surface with hand sander or small grinding tool, using fine stones to achieve desired finish.

Use a #40 or finer grit stone for the initial grinding, exposing the marble chips. Follow with a fine #80 grit stone before grouting with cement to fill all pinholes.

Be careful grinding around dividing strips.

Cover grouted surface with paper or polyethylene for at least 72 hours.

Thoroughly rinse the surface with clean water; remove excess water.

Machine- or hand-apply grout using matching Portland Cement, filling all voids completely.

Final polish with a #80 or finer grit stone. Care should be taken to limit grinding and polishing to a small distance beyond the perimeter of the patch.

Seal patch with a colorless, slip and stain resistant penetrating sealer with pH factor between 7 and 10, that does not affect color or physical properties of the terrazzo.

Epoxy Patching Cracks in Terrazzo Floors

Remove all foreign matter from the void, followed by routing with a power tool. Remove all sealer from the surface adjacent to the void with a stripper or ammonia.

Blend the resin materials, matching the color and aggregate size of existing terrazzo.

Force mixed resin into the void, making sure it is pressured into the crack as deep as possible. Marble chips can be added to the mixture while it is still wet to match existing terrazzo blend. Tool off surface and allow to cure.

When the material has hardened, sand surface with a hand sander or small grinding tool, using fine stones.

Use a #40 or finer grit stone for the initial grinding, exposing the marble chips. Follow with a fine #80 grit stone before grouting with cement to fill all pinholes.

Be careful grinding around dividing strips.

Cover grouted surface with paper or polyethylene for at least 72 hours.

Thoroughly rinse the surface with clean water; remove excess water and allow to dry.

Final polish with a #80 or finer grit stone. Care should be taken to limit grinding and polishing to a small distance beyond the perimeter of the patch.

For some time, this area will be noticeable, however, with normal maintenance, the area will blend into the balance of the floor.

See the GSA Historic Preservation Technical Procedures titled, "Patching Minor Chips And Cracks In Terrazzo With Cement Grout" and "Epoxy Patching Cracks In Terrazzo Floors," found on the GSA web site at http://w3.gsa.gov/web/p/hptp.nsf?OpenDatabase, for detailed information on products, manufacturers, and procedures.

Installing a New Bonded Terrazzo Floor to Match Historic Terrazzo

If may be necessary to install a new terrazzo floor to replace lost or severely damaged portions of existing terrazzo floors, or to enlarge or alter an area of existing/historic terrazzo flooring. This work requires professional, experienced technicians and special procedures.

Examine the existing floor to determine type of terrazzo in order to match marble chips and matrix by size, mineral content, and color for replication and replacement. Color samples should be taken after existing floor has been cleaned. Thoroughly examine the existing conditions of floor to determine necessary work.

Match the historic character and pattern of the terrazzo in all spaces containing or contiguous with existing terrazzo. Provide terrazzo bases, thresholds, stair treads and landings, without interruptions of seams, except where divider strips, control joints, and expansion joints are required. Place and finish terrazzo around obstructions to achieve continuous color, pattern, and finish.

See the GSA Historic Preservation Technical Procedure titled, "Installing A New Bonded Terrazzo Floor To Match Historic Terrazzo," found on the GSA web site at http://w3.gsa.gov/web/p/hptp.nsf?OpenDatabase, for detailed information on products, manufacturers, and procedures.

For further information on maintaining, cleaning, and restoring terrazzo floors, refer to the GSA Historic Preservation Technical Procedures found on the GSA web site at http://www.gsa.gov/historicpreservation. The complete list of topics included:

TERRAZZO:

Terrazzo: Characteristics, Uses And Problems

Routine Preventive Maintenance Guidelines For Terrazzo

Stripping And Cleaning Dirty Or Discolored Terrazzo Floors

Removing Ink Stains From Terrazzo Floors

Removing Lubricating Oil Stains From Terrazzo Floors

Removing Tobacco Stains From Terrazzo Floors

Removing Coffee Stains From Terrazzo Floors

Removing Iodine Stains From Terrazzo Floors

Stripping Built-Up Floor Coatings From Terrazzo

Patching Minor Chips And Cracks In Terrazzo With Cement Grout

Epoxy Patching Cracks In Terrazzo Floors

Regrinding Terrazzo Floors

Installing A New Bonded Terrazzo Floor To Match Historic Terrazzo