03M01/02/08

S153-03M.doc

Use on all projects.

Section 153. - CONTRACTOR QUALITY CONTROL

Construction Requirements

153.02  Contractor Quality Control Plan.

(a) Process control testing.  Add the following:

See Table 153-1 for schedule of minimum sampling and testing for process control.  Where no minimums are specified, submit proposed tests to be performed and the proposed sampling and testing frequencies.

For aggregates and/or aggregate/asphalt mixtures accepted under Subsection 106.03, sample and test for conformity with the Certification a minimum of one time per pay item.

(b) Inspection/control procedures.

(3) Production phase.  Add the following:

(d) Inspect the work, materials or assemblies accepted under Subsection 106.03 to ensure that all the work and materials comply with contract requirements.  Furnish the results of the work inspection, along with the product certification or commercial certification as applicable, to the CO prior to incorporating the materials into the work.

(c) Description of records.  Add the following:

Identify the format for reporting test results, materials certifications and the procedures to be used to maintain inspection records.

On small jobs (i.e. ERFO, OMAD etc), check with the COE regarding the need for a QCS that is separate from the Contractor’s Superintendent. If a separate QCS is not needed, do not include the second sentence which states; “The QCS will not be the Contractor’s Superintendent.”

(d) Personnel qualifications.

(1) Add the following:

Designate a Quality Control Supervisor (QCS) whose primary responsibility is managing the inspection system.  The QCS will not be the Contractor's Superintendent.  Designate a QCS who is experienced to perform and supervise all work inspection, sampling and testing.  The QCS will monitor all phases of the work and identify deficiencies and take appropriate corrective action.

Add the following:

(3) Personnel assigned to sampling or testing will have 1 year or more of recent job experience in the type of sampling and testing required by the contract, and the following:

(a) NICET Level II certification in highway materials, or State (SHA) or industry certification-related sampling and testing equivalent to their intended responsibilities.

(b) WAQTC or other nationally accepted certification program for intended sampling and testing responsibilities.

or

(c) Current or previous employment by an AASHTO accredited laboratory performing sampling and testing equivalent to their intended responsibilities.

(d) Demonstrated proficiency or successful testing of one or more proficiency samples may be substituted for basic qualifications pending verification of test results.

153.03  Testing.  Delete the title and text and substitute the following:

153.03  Sampling and Testing.  Perform the work required by Table 153-1 and by the accepted Quality Control Plan.

(a) Acceptance sampling.  Acceptance sampling schedules and times or locations will be provided by the CO.  Use a procedure for random sampling.  In addition, sample any material that appears defective or inconsistent with similar material being produced, unless such material is voluntarily removed and replaced or otherwise corrected.

(b) Testing.  If the Government-furnished field laboratory option is not exercised by the CO, furnish a laboratory equipped with all test equipment necessary to satisfy the requirements of the contract.  Ensure test equipment has been checked, calibrated, standardized and/or otherwise verified in accordance with AASHTO and ASTM standards by an individual qualified to do this work.  Ensure mobile laboratories receive an equipment inspection after the laboratory has been moved to its permanent location on the project site and anytime it is moved thereafter.  Inspect equipment within 45 days of actual use in project testing and at least once a year thereafter.  Do not use equipment that has not been inspected or is found to be deficient.  Mark deficient equipment and take it out-of-service until it is repaired or replaced and shown by subsequent inspection to perform as required.  Maintain records documenting these inspections in the laboratory.  Provide certification(s) stating the equipment conforms to testing requirements and provide evidence of current inspection.

The CO may require the Contractor to perform testing to demonstrate acceptable equipment and an acceptable level of technician competence.  The CO may also check equipment and inspection records to verify condition.  Repair or replace equipment not meeting applicable requirements.  Keep laboratory facilities clean and maintain equipment in proper working condition.  Provide the CO unrestricted access to the laboratory for inspection and review.

(c) Certifications.  For materials accepted by certification in accordance with 106.03, review all certifications to insure compliance with the requirements of the contract prior to incorporating materials into the work and provide a signed copy of the reviewed certification(s) to the CO.

153.04  Records.  Add the following to the first paragraph:

When tests are on material being incorporated into the work, report test results within the reporting times indicated in the sampling and testing requirements at the end of each section or as specified in the contract.

Add the following to the second paragraph:

Detailed inspection results including deficiencies observed and corrective actions taken.

153.05  Acceptance.  Add the following:

If chronic deficiencies are noted in the Contractor's inspection or testing systems, the CO may order supplemental inspection and/or testing to be performed.  The Government will charge to the Contractor all costs associated with such supplemental inspection or testing.

The Section 153.07 pay item is rarely used. Include Subsections 153.06 and 07 when there is a bid item for 153. If 154 (Contractor Sampling and Testing) is a bid item, do not include subsections 153.06 and 153.07.

Delete the text for Measurement and Payment and substitute the following:

Measurement

153.06  Contractor quality control will be measured by the lump sum.

Payment

153.07  The accepted quantity, measured as provided above, will be paid at the contract price per unit of measurement for the pay item listed below that is shown in the bid schedule.  Payment will be full compensation for the work prescribed in this Section.  See Subsection 109.05.

The Contractor quality control lump sum will be paid as follows:

- 25 percent of the lump sum, not to exceed 0.5 percent of the original contract amount, will be paid after all testing facilities are in place, qualified sampling and testing personnel have been identified, and the work being tested has started.

- Payment for the remaining portion of the lump sum will be prorated based on the total work completed.

Include all Tables on all projects.

Table 153-1

Schedule of Minimum Sampling and Testing For Process Control

(to be performed by the Contractor)

Section(s):  204, 208, 209.

| Material | Property or Characteristic | Test Method or Specification | Frequency | Sampling Point |
| --- | --- | --- | --- | --- |
| Embankment Construction Composition of Roadbed in Cuts | Classification and Moisture/Density | AASTHO M 145 AASHTO T 99 or AASTHO T 180 (minimum of 5 proctor points). | 1 per material/type. | Source of material. |
|  | In-place density and moisture content | AASHTO T 310 | 2 per lift, but not less than 2 every 800 cubic meters. | Compacted embankment, subgrade as applicable. |
|  | R-value | AASHTO T 190 (Tested by FHWA Central Lab). | 1 per 700 meters, or change in material type. | Sample depth: 0-300 mm. |
| Bedding/Backfill for Structures and Culvert Pipe | Classification and Moisture/Density | AASTHO M 145 AASHTO T 99 or AASTHO T 180 (minimum of 5 proctor points). | 1 per material/type. | Source of material. |
|  | In-place density and moisture content | AASHTO T 310 | 1 per 15 meters/lift. Minimum 2 per lift. | Compacted bedding or backfill as applicable. |

Include all Tables on all projects.

Table 153-1

Schedule of Minimum Sampling and Testing For Process Control

(to be performed by the Contractor)

Section(s):  255.

| Material | Property or Characteristic | Test Method or Specification | Frequency | Sampling Point |
| --- | --- | --- | --- | --- |
| Select wall backfill 704.13(a) and Wall backfill 704.13(b) | Gradation and liquid limit | AASHTO T 11 AASHTO T 27 AASHTO T 89 AASHTO T 90 | 1 per material/type | Source of material |
|  | Moisture Density | AASHTO T99, Method C (1) | 1 per material/type | Source of material |
|  | In-place density and moisture content | AASHTO T 310 | For MSE walls: 1 per 300-mm lift per 75-meters of wall length (minimum of 2 per lift) | Compacted backfill |

(1) A minimum of 5 points are required for moisture density test.

Include all Tables on all projects.

Table 153-1

Schedule of Minimum Sampling and Testing For Process Control

(to be performed by the Contractor)

Section(s):  301, 303, 304, 305, 306, 308.

| Material | Property or Characteristic | Test Method or Specification | Frequency | Sampling Point |
| --- | --- | --- | --- | --- |
| Subbase, Base Course Aggregate Stabilization and Aggregate Topsoil Courses | Gradation (301) | AASTHO T 11 AASTHO T 27 | 2 per day | Crusher belt |
|  | Moisture/Density | AASHTO T 99 or AASTHO T 180 (minimum of 5 proctor points) | 1 per source of material | Source of material |
|  | In-place density and moisture content | AASHTO T 310 or ASTM 2950 | 2 per lift at 300-meter intervals, alternating lanes | Compacted aggregate |
|  | Plasticity index (aggregate surfacing only) | AASHTO T 90 | 2 per day | Crusher belt |
|  | Gradation (304 materials processed in place) | AASHTO T 11 AASHTO T 27 | 1 per 300 meters | Processed material |
| Magnesium Chloride and Calcium Chloride | Specific Gravity | Hydrometer | 1 per shipment | Transport vehicle |

Note:  Density and Moisture calculations AASHTO T 310...Density corrections based on moisture for recycled materials containing asphalts, or aggregates containing MgCl or CaCl will be made based on samples taken from each test site and oven-dried in the laboratory.

Include all Tables on all projects.

Table 153-1

Schedule of Minimum Sampling and Testing For Process Control

(to be performed by the Contractor)

Section:  401.

| Material | Property or Characteristic | Test Method or Specification | Frequency | Sampling Point |
| --- | --- | --- | --- | --- |
| Superpave Hot Asphalt Concrete Pavement | Gradation | AASTHO T 11 AASHTO T 27 | 2 per day per stockpile | Crusher belt (during production) and Cold Feed or Hot Bins (as applicable during production of hot mix) |
|  | Moisture content of aggregates | AASHTO T 255 | 1 per day | Cold Feed (during production of hot mix) |
|  | Compaction | ASTM D2950 | Test strip, first day of production to establish roller pattern: 12 per 500 meters, then 3 per 500 meters | In place, after compaction |
|  | Placement temperature | Thermometer | As directed | Behind laydown machine |
|  | Surface tolerance | Straight edge and FLH T 504 | During and after compaction | See Subsection 401.16 |
| Aggregate | Fine aggregate angularity | AASHTO T 304, Method A | 1 per day | Cold Feed |

Include all Tables on all projects.

Table 153-1

Schedule of Minimum Sampling and Testing For Process Control

(to be performed by the Contractor)

Section(s):  402, 403, 404, 405, 408.

| Material | Property or Characteristic | Test Method or Specification | Frequency | Sampling Point |
| --- | --- | --- | --- | --- |
| Asphalt Concrete Pavement Open-Graded Asphalt Friction Course Asphalt Base Course | Gradation | AASTHO T 11 AASHTO T 27 | 2 per day per stockpile | Crusher belt (during production) and Cold Feed or Hot Bins (as applicable during production of hot mix) |
|  | Moisture content of aggregates | AASHTO T 255 | 1 per day | Cold Feed (during production of hot mix) |
|  | Compaction | ASTM D2950 | Test strip, first day of production to establish roller pattern: 12 per 500 meters, then 3 per 500 meters | In place, after compaction |
|  | Placement temperature | Thermometer | As directed | Behind laydown machine |
|  | Surface tolerance | Straight edge and FLH T 504 | During and after compaction | See Subsection 401.16 |

Include all Tables on all projects.

Table 153-1

Schedule of Minimum Sampling and Testing For Process Control

(to be performed by the Contractor)

Section(s):  409, 410.

| Material | Property or Characteristic | Test Method or Specification | Frequency | Sampling Point |
| --- | --- | --- | --- | --- |
| Chip seal aggregate Slurry seal aggregate | Gradation | AASTHO T 11 AASHTO T 27 | 2 per day | Production belt or spreader discharge |
|  | Moisture content of aggregates | AASHTO T 255 | 1 per day | Stockpile or spreader discharge |
| Asphalt binder Emulsified asphalt | Placement temperature | Thermometer | Prior to each days production, followed by 2 each day | Distributor truck |

Include all Tables on all projects.

Table 153-1

Schedule of Minimum Sampling and Testing For Process Control

(to be performed by the Contractor)

Section(s):  416, 418.

| Material | Property or Characteristic | Test Method or Specification | Frequency | Sampling Point |
| --- | --- | --- | --- | --- |
| Continuous Cold Recycled Asphalt Base Course Foamed Asphalt Stabilized Base Course | Gradation | AASTHO T 27 (maximum size only) | 1 per 500 meters | Recycled material prior to compaction |
|  | Moisture content | FLH T 515 | Minimum 1 per 500 meters alternating lanes (as necessary to comply with contract requirements) | In place after compaction and prior to compaction to determine total moisture. |
|  | In-place density | ASTM D2950 | 1 per 500 meters, alternating lanes (1 value will be equal to the mean of 3 in-place tests, and as necessary to comply with contract requirements) | In place after compaction |

Note:  Density and Moisture calculations ASTM D 2950...Density corrections based on moisture for recycled materials containing asphalts, or aggregates containing MgCl or CaCl will be made based on samples taken from each test site and oven-dried in the laboratory.

Include all Tables on all projects.

Table 153-1

Schedule of Minimum Sampling and Testing For Process Control

(to be performed by the Contractor)

Section(s):  501, 552, 601.

| Material | Property or Characteristic | Test Method or Specification | Frequency | Sampling Point |
| --- | --- | --- | --- | --- |
| Concrete | Gradation and fineness modulus | AASTHO T 11 AASHTO T 27 | 1 per day | Aggregate, before batching |
|  | Moisture | AASHTO T 255 | 1 per day/stockpile | Aggregate, before batching |
|  | Slump | AASHTO T 119 | 1 per 25 cubic meters, minimum 1 per day | See note |
|  | Air content | AASHTO T 152 | 1 per 25 cubic meters, minimum 1 per day | See note |
|  | Unit weight | AASHTO T 121 | 1 per 25 cubic meters, minimum 1 per day | See note |
|  | Temperature | Thermometer | 1 per 25 cubic meters, minimum 1 per day | See note |
|  | Making test specimens for compressive strength | AASHTO T 23 | 1 set per 25 cubic meters, minimum 1 set per day | At point of discharge |

Note:  If an extended set admixture is used for the sole purpose of extending discharge times, sampling and testing will be performed by the Contractor at point of batching and discharge location to ensure compliance with Subsection 552.08.