# PART VII – MISCELLANEOUS

### ITEM P-602  BITUMINOUS PRIME COAT

DESCRIPTION

602-1.1  This item shall consist of an application of bituminous  material on the prepared base course in accordance with these specifications and in reasonably close conformity to the lines shown on the plans.

MATERIALS

602-2.1  BITUMINOUS MATERIAL.  The types, grades, controlling specifications, and application temperatures for the bituminous materials are given in Table 1.  The Engineer shall designate the specific material to be used.

TABLE 1.  BITUMINOUS MATERIAL

|  |  | Application Temperatures \1\ |
| --- | --- | --- |
| Type and Grade | Specification | Deg. F | Deg. C |
| Emulsified Asphalt |  |  |  |
| SS-1, SS-1h | ASTM D 977 | 70-160 | 20-70 |
| MS-2, HFMS-1 | ASTM D 977 | 70-160 | 20-70 |
| CSS-1, CSS-1h | ASTM D 2397 | 70-160 | 20-70 |
| CMS-2 | ASTM D 2397 | 70-160 | 20-70 |
| Cutback Asphalt |  |  |  |
| RC-30 | ASTM D 2028 | 80+ | 30+ |
| RC-70 | ASTM D 2028 | 120+ | 50+ |
| RC-250 | ASTM D 2028 | 165+ | 75+ |

\1\  The maximum temperature for cutback asphalt shall be that at which fogging occurs.

CONSTRUCTION METHODS

602-3.1  WEATHER LIMITATIONS.  The prime coat shall be applied only when the existing surface is dry or contains sufficient moisture to get uniform distribution of the bituminous material, when the atmospheric temperature is above 60°F (15°C), and when the weather is not foggy or rainy.  The temperature requirements may be waived, but only when so directed by the Engineer.

602-3.2  EQUIPMENT.  The equipment used by the Contractor shall include a self-powered pressure bituminous material distributor and equipment for heating bituminous material.

The distributor shall be designed, equipped, maintained, and operated so that bituminous material at even heat may be applied uniformly on variable widths of surface at the specified rate.  The allowable variation from the specified rate shall not exceed 10 percent.  Distributor equipment shall include a tachometer, pressure gages, volume-measuring devices or a calibrated tank, and a thermometer for measuring temperatures of tank contents.  The distributor shall be self-powered and shall be equipped with a power unit for the pump and full circulation spray bars adjustable laterally and vertically.

If the distributor is not equipped with an operable quick shut off valve, the prime operations shall be started and stopped on building power.  The Contractor shall remove blotting sand prior to asphalt concrete lay down operations at no additional expense to the owner.

A power broom and/or blower shall be provided for any required cleaning of the surface to be treated.

602-3.3  APPLICATION OF BITUMINOUS MATERIAL.  Immediately before applying the prime coat, the full width of the surface to be primed shall be swept with a power broom to remove all loose dirt and other objectionable material.

The bituminous material including solvent shall be uniformly applied with a bituminous distributor at the rate of 0.25 to 0.50 gallons per square yard (1.20 to 2.40 liters per square meter) depending on the base course surface texture.  The type of bituminous material and application rate shall be approved by the Engineer prior to application.

Following the application, the primed surface shall be allowed to dry not less than 48 hours without being disturbed or for such additional time as may be necessary to permit the drying out of the prime coat until it will not be picked up by traffic or equipment.  This period shall be determined by the Engineer.  The surface shall then be maintained by the Contractor until the surfacing has been placed.  Suitable precautions shall be taken by the Contractor to protect the primed surface against damage during this interval, including supplying and spreading any sand necessary to blot up excess bituminous material.

602-3.4  BITUMINOUS MATERIAL CONTRACTOR'S RESPONSIBILITY.  Samples of the bituminous materials that the Contractor proposes to use, together with a statement as to their source and character, must be submitted and approved before use of such material begins.  The Contractor shall require the manufacturer or producer of the bituminous materials to furnish material subject to this and all other pertinent requirements of the contract.  Only satisfactory materials, so demonstrated by service tests, shall be acceptable.

The Contractor shall furnish vendor's certified test reports for each carload, or equivalent, of bituminous material shipped to the project.  The test reports shall contain all the data required by the applicable specification.  If the Contractor applies the prime material prior to receipt of the tests reports, payment for the material shall be withheld until they are received.  If the material does not pass the specifications it shall be replaced at the contractor's expense.   The report shall be delivered to the Engineer before permission is granted for use of the material.  The furnishing of the vendor's certified test report for the bituminous material shall not be interpreted as basis for final acceptance.  All such test reports shall be subject to verification by testing samples of materials received for use on the project.

602-3.5  FREIGHT AND WEIGH BILLS.  Before the final estimate is allowed, the Contractor shall file with the Engineer receipted bills when railroad shipments are made, and certified weigh bills when materials are received in any other manner, of the bituminous materials actually used in the construction covered by the contract.  The Contractor shall not remove bituminous material from the tank car or storage tank until the initial outage and temperature measurements have been taken by the Engineer, nor shall the car or tank be released until the final outage has been taken by the Engineer.

Copies of freight bills and weigh bills shall be furnished to the Engineer during the progress of the work.

METHOD OF MEASUREMENT

602-4.1  The bituminous material for prime coat shall be measured by the [gallon (liter)][ton(kg)] .  Volume shall be corrected to the volume at 60°F (15°C) in accordance with ASTM D 1250 for cutback asphalt, and Table IV-3 of The Asphalt Institute's Manual MS-6 for emulsified asphalt.

BASIS OF PAYMENT

602-5.1  Payment shall be made at the contract unit price per [gallon (liter)][ton (kg)]  for bituminous prime coat.  This price shall be full compensation for furnishing all materials and for all preparation, delivering, and applying the materials, and for all labor, equipment, tools, and incidentals necessary to complete this item.

Payment will be made under:

Item P-602-5.1	Bituminous Prime Coat—per [gallon (liter)][ton (kg)]

MATERIAL REQUIREMENTS

ASTM D 977		Emulsified Asphalt

ASTM D 2028		Cutback Asphalt (Rapid Curing Type)

ASTM D 2397		Cationic Emulsified Asphalt

TESTING REQUIREMENTS

ASTM D 1250		Petroleum Measurement Tables

Asphalt Institute		Asphalt Pocketbook of Useful Information (Temperature-Volume Corrections

Manual MS-6    		for Emulsified Asphalts)

Table IV-3

END OF ITEM P-602

Intentionally Left Blank