# PART IV – RIGID BASE COURSES

### ITEM P-301  SOIL-CEMENT BASE COURSE

DESCRIPTION

301-1.1   This item shall consist of constructing a base course by uniformly mixing together soil, portland cement, and water.  The mixed material shall be spread, shaped, and compacted in accordance with these specifications and in conformity to the dimensions and typical cross section shown on the plans.  Tests shall be required for each approved soil that will be included in the treated layer.

Runway, taxiway, or apron pavements shall be built in a series of parallel lanes using a plan of processing that reduces longitudinal and transverse joints to a minimum.

MATERIALS

301-2.1  PORTLAND CEMENT.  Portland cement shall conform to the requirements of ASTM [    ].

* * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * *

The Engineer shall specify ASTM C 150, Type I, II, III, IV, or IV.

* * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * *

301-2.2  WATER.  Water shall be clean and free from sewage, oil, acid, strong alkalies, or vegetable matter.  Water of questionable quality shall be tested in accordance with the requirements of AASHTO T 26.

301-2.3  SOIL.  The soil shall consist of an approved select soil.  The soil shall be free of roots, sod, weeds, and shall not contain gravel or stone retained on a 1-inch (25 mm) sieve or more than 45% retained on a No. 4 sieve, as determined by ASTM C 136.

301-2.4  BITUMINOUS MATERIAL.  The types, grades, controlling specifications, and application temperatures for the bituminous materials used for curing the soil-cement are listed in Table 1.  The Engineer shall designate the specific material used.

TABLE 1.  BITUMINOUS MATERIALS

| Type and Grade | Specification | Application Temperature |
| --- | --- | --- |
|  |  | Deg. F | Deg. C |
| Cutback Asphalt |  |  |  |
| RC-70 | ASTM D 2028 | 120-160 | 50-70 |
| RC-250 | ASTM D 2028 | 160-200 | 70-95 |
| Emulsified Asphalt |  |  |  |
| RS-1, SS-1 | ASTM D 977 | 75-130 | 25-55 |
| CRS-1 | ASTM D 2397 | 75-130 | 25-55 |

CEMENT QUANTITY

301-3.1  LABORATORY SOIL TESTS.  Prior to base course construction, laboratory tests of soils shall be made to determine the quantity of cement required in the mix.

Test specimens containing various amounts of cement are to be compacted in accordance with ASTM D 558, and the optimum moisture for each amount of cement is to be determined.  Samples at the optimum moisture shall be subjected to the wet-dry and the freeze-thaw test in accordance with ASTM D 559 and D 560, respectively.

The specified cement content for construction shall be that at which the weight loss of the specimens subjected to 12 cycles of either the wet-dry or the freeze-thaw is not more than 14% for granular soils, 10% for the more plastic granular and silty soils, and 7% for clay soils.

The compressive strength of soaked specimens should increase both with age and with increase in cement content.

CONSTRUCTION METHODS

301-4.1  WEATHER LIMITATIONS.  The soil-cement base shall not be mixed or placed while the atmospheric temperature is below 35° F (2° C) or when conditions indicate that the temperature may fall below 35° F (2° C) within 24 hours, or when the weather is foggy or rainy, or when the soil or subgrade is frozen.

301-4.2  EQUIPMENT.  The soil-cement may be constructed with any equipment that will meet the requirements for soil pulverization, cement application, mixing, water application, incorporation of materials, compaction, finishing, and curing specified herein.

301-4.3  PREPARATION.  The area to be paved shall be graded and shaped to conform to the grades and typical cross section shown on the plans.  Any soft or yielding areas in the subgrade shall be removed and replaced with acceptable soil and compacted as specified.

301-4.4  PULVERIZATION.  The soil for the base course shall be so pulverized that at the completion of moist-mixing, 100% by dry weight passes a 1-inch (25 mm) sieve and a minimum of 80% passes a No. 4 sieve, exclusive of gravel or stone retained on the No. 4 sieve.

301-4.5  CEMENT APPLICATION, MIXING, AND SPREADING.  Mixing of the soil, cement, and water shall be accomplished either by the mixed-in-place or the central-plant-mixed method.

The percentage of moisture in the soil, at the time of cement application, shall not exceed the quantity that will permit a uniform and intimate mixture of soil and cement during mixing operations, and it shall not exceed the specified optimum moisture content for the soil-cement mixture.

Method A – Mixed-in-place.  The specified quantity of cement shall be spread uniformly on the soil.

Cement that has been displaced shall be replaced before mixing is started.  After the cement has been applied, it shall be mixed with the soil.  Mixing shall continue until the cement has been sufficiently blended with the soil to prevent the formation of cement balls when water is applied.

Immediately after the soil and cement have been mixed, water shall be incorporated into the mixture.  Excessive concentrations of water on or near the surface shall be avoided.  A water supply and pressure distributing equipment shall be provided that will assure the application within 3 hours of all mixing water on the section being processed.  After all mixing water has been applied, mixing shall continue until a uniform and intimate mixture of soil, cement, and water has been obtained.

Method B – Central plant mixed.  The soil, cement, and water shall be mixed in a pugmill, either of the batch or continuous-flow type.  The plant shall be equipped with feeding and metering devices that will add the soil, cement, and water into the mixer in the specified quantities.  Soil and cement shall be mixed sufficiently to prevent cement balls from forming when water is added.  Mixing shall continue until a uniform and intimate mixture of soil, cement, and water is obtained.

The mixture shall be hauled to the project in trucks equipped with protective covers.  The mixture shall be placed on the moistened subgrade in a uniform layer by an approved spreader(s).  Not more than 30 minutes shall elapse between the placement of soil-cement in adjacent lanes.

The layer of soil-cement shall be uniform in thickness and surface contour and of such quantity that the completed base will conform to the required grade and cross section.  Dumping of the mixture in piles or windrows upon the subgrade will not be permitted.

Not more than 60 minutes shall elapse between the start of moist mixing and the start of compaction of soil-cement.

301-4.6  COMPACTION.  Immediately upon completion of the spreading operations, the mixture shall be thoroughly compacted.  The number, type, and weight of rollers shall be sufficient to compact the mixture to the required density.

The field density of the compacted mixture shall be at least 98 percent of the maximum density of laboratory specimens prepared from samples of the cement-treated base material taken from the material in place.  The specimens shall be compacted and tested in accordance with ASTM D 558.  The in-place field density shall be determined in accordance with ASTM D 1556.  Any mixture that has not been compacted shall not be left undisturbed for more than 30 minutes.  The moisture content of the mixture at the start of compaction shall not be below nor more than 2 percentage points above the optimum moisture content.  The optimum moisture content shall be determined in accordance with ASTM D 558 and shall be less than that amount which will cause the mixture to become unstable during compaction and finishing.

301-4.7  FINISHING.  Finishing operations shall be completed during daylight hours, and the completed base course shall conform to the required lines, grades, and cross section.  If necessary, the surface shall be lightly scarified to eliminate any imprints made by the compacting or shaping equipment.  The surface shall then be recompacted to the required density.

301-4.8  CONSTRUCTION JOINTS.  At the end of each day's run, a transverse construction joint shall be formed by a header or by cutting back into the compacted material to form a true vertical face free of loose material.

The protection provided for construction joints shall permit the placing, spreading, and compacting of base material without injury to the work previously laid.  Where it is necessary to operate or turn any equipment on the completed base course, sufficient protection and cover shall be provided to prevent damage to the finished surface.  A supply of mats or wooden planks shall be maintained and used as approved and directed by the Engineer.

Care shall be exercised to ensure thorough compaction of the base material immediately adjacent to all construction joints.  When spreading or compacting base material adjacent to a previously constructed lane, care shall be taken to prevent injury to the work already constructed.

301-4.10  PROTECTION AND CURING.  After the base course has been finished to grade and compacted as specified herein, it shall be protected against drying for a period of 7 days by the application of bituminous material or other acceptable methods.  The curing method shall begin as soon as possible, but no later than 24 hours after the completion of finishing operations.  The finished base course shall be kept moist continuously until the curing material is placed.

The bituminous material specified shall be uniformly applied to the surface of the completed base course at the rate of approximately 0.2 gallon  per square yard (0.92 liter/square meter) with approved heating and distributing equipment.  The exact rate and temperature of application to give complete coverage without excessive runoff shall be as specified.

At the time the bituminous material is applied, the surface shall be dense, free of all loose and extraneous material, and shall contain sufficient moisture to prevent penetration of the bituminous material.  Water shall be applied in sufficient quantity to fill the surface voids immediately before the bituminous curing material is applied.

The curing material shall be maintained and applied as needed by the Contractor during the 7-day protection period so that all of the soil-cement will be covered effectively during this period.

Finished portions of soil-cement that are used by equipment in constructing an adjoining section shall be protected to prevent equipment from marring or damaging the completed work.

When the air temperature may be expected to reach the freezing point, sufficient protection from freezing shall be given the soil-cement for 7 days after its construction and until it has hardened.

Other curing materials such as moist straw or hay may be used if approved.

301-4.11  CONSTRUCTION LIMITATIONS.  When any of the operations after the application of cement are interrupted for more than 30 minutes or when the uncompacted soil-cement mixture is wetted by rain so that the moisture content is exceeded by a small amount, the decision to reconstruct the portion affected shall rest with the Engineer.  In the event the uncompacted, rain-wetted mixture exceeds the specified moisture content tolerance, the Contractor shall reconstruct at his/her expense the portion affected.  All material along the longitudinal or transverse construction joints not properly compacted shall be removed and replaced, at the Contractor's expense, with properly moistened and mixed soil-cement compacted to specified density.

301-4.12  SURFACE TESTS.  The finished surface shall not vary more than 3/8 inch (9 mm) when tested with a 16-foot (4.8 m) straightedge applied parallel with, or at right angles to, the longitudinal axis of the pavement.  Any variations in excess of this tolerance shall be corrected by the Contractor, at his/her own expense, and in a manner satisfactory to the Engineer.

301-4.13  THICKNESS.  The thickness of the soil-cement base course shall be determined from measurements of cores drilled from the finished base or from thickness measurements at holes drilled in the base at intervals so that each test shall represent no more than 300 square yards (250 square meters).  The average thickness of the base constructed during one day shall be within 1/2 inch (12 mm) of the thickness shown on the plans, except that the thickness of any one point may be within 3/4 inch (13 mm) of that shown on the plans.  Where the average thickness shown by the measurements made in one day's construction is not within the tolerance given, the Engineer shall evaluate the area and determine if, in his/her opinion, it shall be reconstructed at the Contractor's expense or the deficiency deducted from the total material in place.

301-4.14  MAINTENANCE.  The Contractor shall be required to maintain, at his/her own expense, the entire base course within the limits of his/her contract in a condition satisfactory to the Engineer from the time he starts work until all the work has been completed.  Maintenance shall include immediate repairs of any defects that may occur either before or after the cement is applied.  The work shall be done by the Contractor at his/her own expense and repeated as often as necessary to keep the area intact at all times.  Repairs shall be made in a manner that will insure restoration of a uniform surface and the durability of the part repaired.  Faulty work must be replaced for the full depth of treatment.  Any low areas shall be remedied by replacing the material for the full depth of treatment rather than by adding a thin layer of soil-cement to the completed work.

METHOD OF MEASUREMENT

301-5.1  The quantity of soil-cement base course to be paid for shall be the number of square yards (square meters) of completed and accepted base course.

301-5.2  Portland cement shall be measured by the hundredweight.

BASIS OF PAYMENT

301-6.1  Payment shall be made at the contract unit price per square yard (square meter) for soil-cement base course.  This price shall be full compensation for furnishing all materials, except portland cement, and for all preparation, delivering, placing, and mixing of these materials; and for all labor, equipment, tools and incidentals necessary to complete the item.

301-6.2  Payment shall be made at the contract unit price per hundredweight for cement. This price shall be full compensation for furnishing this material and for all delivery, placing, and incorporation of this material, and for all labor, equipment, tools, and incidentals necessary to complete the item.

Payment will be made under:

Item P-301-6.1	Soil-Cement Base Course—per square yard (square meter)

Item P-301-6.2	Portland Cement—per hundredweight

TEST REQUIREMENTS

ASTM C 136	Sieve Analysis of Fine and Coarse Aggregates

ASTM D 558	Moisture-Density Relations of Soil-Cement Mixtures

ASTM D 559	Wetting-and-Drying Tests of Compacted Soil-Cement Mixtures

ASTM D 560	Freezing-and-Thawing Tests of Compacted Soil-Cement Mixtures

ASTM D 1556	Test for Density of Soil In-Place by the Sand Cone Method

AASHTO T 26	Quality of Water to be Used in Concrete

MATERIAL REQUIREMENTS

ASTM C 150	Portland Cement

ASTM D 977	Emulsified Asphalt

ASTM D 202	Cutback Asphalt

ASTM D 239	Cationic Emulsified Asphalt

END OF ITEM P-301

Intentionally Left Blank

### ITEM P-304  CEMENT-TREATED BASE COUSE

#### DESCRIPTION

304-1.1  This item shall consist of a cement-treated base (CTB) course composed of mineral aggregate and cement, uniformly blended and mixed with water.  The mixed material shall be spread and shaped with a mechanical spreader, and compacted with rollers in accordance with these specifications and in conformance to the lines, grades, dimensions, and cross-sections shown on the plans.

#### MATERIALS

304-2.1  AGGREGATE.  The aggregate shall be select granular materials, comprised of crushed or uncrushed gravel and/or stone, or recycled crushed and graded portland cement concrete (PCC).  The material shall be free of roots, sod, and weeds.  The crushed or uncrushed aggregate shall consist of hard, durable particles of accepted quality, free from an excess of soft, flat, elongated, or disintegrated pieces, and objectionable matter.  The method used in producing the aggregate shall be such that the finished product is as consistent as practicable.  All stones and rocks of inferior quality shall be wasted.  When recycled PCC is used as the aggregate, it must meet the requirements for virgin aggregate.

The percentage of wear of the crushed aggregate retained on the No. 4 (4.75-mm) sieve shall not be greater than 40 percent when tested in accordance with ASTM C 131.  The sodium sulfate soundness loss shall not exceed 10 percent, or the magnesium sulfate soundness loss shall not exceed 13 percent, after five cycles, when tested in accordance with ASTM C 88.

When tested in accordance with ASTM C 136, the aggregate shall conform to the gradations shown in Table 1.  An aggregate blend that meets the requirements of Table 1 shall be selected by the Contractor and used in the final mix design.  The final aggregate blend shall be well graded from coarse to fine within the limits designated in the table and shall not vary from the low limit on one sieve to the high limit on adjacent sieves, or vice versa.  The portion of final aggregate blend passing the No. 40 (425-µm) sieve shall have a liquid limit of not more than 25 and a plasticity index of not more than 6 when tested in accordance with ASTM D 4318.

Table 1.  Aggregate gradation for CTB material.

| Sieve Size | Percentage by Weight Passing Sieves |
| --- | --- |
|  | Gradation A | Gradation B |
| 2 in (51 mm) | 100 1 | 100 1 |
| No. 4 (4.75 mm) | 45 - 100 | 55 - 100 |
| No. 10 (1.80 mm) | 37 - 80 | 45 - 100 |
| No. 40 (450 (m) | 15 - 50 | 25 - 80 |
| No. 80 (210 (m) | 0 - 25 | 10 - 35 |

1  Maximum size of aggregate is 1 in (25.4 mm) when used as a base

course under Item P-501, Portland Cement Concrete Pavement.

All aggregate samples required for testing shall be furnished by the Contractor at the expense of the Contractor.  Sampling shall be performed by the Contractor in accordance with ASTM D 75.

304-2.2  CEMENT.  Cement shall conform to the requirements of ASTM [    ].

* * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * *

The Engineer shall specify ASTM C 150 Type I, II, III, IV, or V or ASTM C 595 Type IS, IS-A, IP, IP-A, P, or PA.  Type II cement shall be specified in areas with a history of sulfate reaction with the selected aggregate.

* * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * *

304-2.3  CEMENTITIOUS ADDITIVIES.  Pozzolanic and ground granulated blast furnace (GGBF) slag may be added to the CTB mix.  If used, each material must meet the following requirements:

- Pozzolan.  Pozzolanic materials must meet the requirements of ASTM C 618, Class C, F, or N with the exception of loss of ignition, where the maximum shall be less than 6 percent for Class F or N.  [The supplementary optional chemical and physical properties of tables 1A and 2A contained in ASTM C 618 shall apply].

- GGBF Slag.  Slag shall conform to ASTM C 989, Grade 80, 100, or 120.

304-2.4  WATER.  Water used in mixing or curing shall be clean and free of oil, salt, acid, alkali, sugar, vegetable, or other deleterious substances injurious to the finished product.  Water shall be tested in accordance with the requirements of AASHTO T 26.  Water known to be of potable quality may be used without testing.

304-2.5  CURING MATERIALS.  Curing materials shall conform to the requirements provided below, as defined by the type of pavement surface to be placed on top of the CTB layer.

304-2.5.1  Portland Cement Concrete (PCC) Pavement.  For curing CTB placed under PCC pavement, use white-pigmented, liquid membrane-forming compound conforming to ASTM C 309, Type 2, Class A or Class B (wax-based).

304-2.5.2  Hot Mix Asphalt (HMA) Pavement.  For curing CTB placed under HMA pavement, use emulsified asphalt conforming to ASTM C 977 or ASTM D 2397 (Table 2).

* * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * *

If emulsified asphalt is allowed as a curing agent, the Engineer shall specify

the type and grade of material to be used and the corresponding application temperature from Table 2.

Table 2.  Emulsified asphalt curing material.

| Type and Grade | Specification | Application Temperature |
| --- | --- | --- |
|  |  | °F | °C |
| Emulsified Asphalt |
| RS-1, SS-1 | ASTM D 977 | 75 - 130 | 25 - 55 |
| CRS-1 | ASTM D 2397 | 75 - 130 | 25 - 55 |

* * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * *

304-2.6  SAND BLOTTER.  If emulsified asphalt is used as a curing material, sand shall be applied, when required, for the prevention of pick-up of emulsion curing materials.  The sand material shall be clean, dry, and non-plastic.

#### COMPOSITION OF MIXTURE

304-3.1  GENERAL.  The CTB material shall be composed of a mixture of aggregate, [Portland cement] [blended hydraulic cement], and water.  Fly Ash or GGBF slag may be used as a partial replacement for Portland cement.

304-3.2  MIX DESIGN.  The mix design shall utilize a cement content that, when tested in the laboratory according to ASTM D 1633, produces a 7-day compressive strength meeting the following requirements:

- For CTB placed under PCC pavement:  500 psi (3,447 kPa) minimum and 1,000 psi (6,895 kPa) maximum.

- For CTB placed under HMA pavement:  750 psi (5,170 kPa) minimum and 1,000 psi (6,895 kPa) maximum.

* * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * *

In areas subject to considerable wet-dry and/or freeze-thaw cycles, insert the following statement:

“Wet-dry and/or freeze-thaw tests shall be performed in accordance with ASTM D 559 and D 560, respectively.  The weight loss for each type of test shall not exceed 14 percent after 12 cycles.  However, if a 7-day compressive strength of 750 psi (5,170 kPa) is achieved, the wet-dry and freeze-thaw tests are not necessary.”

An estimated cement content may be determined from Table 1, Chapter 2, of the Soil-Cement Laboratory Handbook, published by the Portland Cement Association (PCA).  In designing the mixture, cement contents above and below the initial estimated amount should be tested to determine the minimum quantity of cement needed to achieve the required strength (or strength and durability where freeze-thaw resistance is deemed necessary by the Engineer).

* * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * *

The mix design shall include a complete list of materials, including type, brand, source, and amount of cement, fine aggregate, coarse aggregate, water, and cementitious additives, if used.  It shall also contain the 7-day compressive strength test results and the results of the wet-dry and/or freeze-thaw tests.

Should a change be made in aggregate sources or type of cement, or if cementitious additives are added or deleted from the mix, production of the CTB mix shall be stopped and a new mix design shall be submitted.

304-3.3  SUBMITTALS.  At least  [    ] days prior to the placement of the CTB, the Contractor shall submit certified test reports to the Engineer for those materials proposed for use during construction, as well as the mix design information for the CTB material.  Tests older than 6 months shall not be used.  The certification shall show the ASTM or AASHTO specifications or tests for the material, the name of the company performing the tests, the date of the tests, the test results, and a statement that the material did or did not comply with the applicable specifications.  The submittal package shall include the following:

- Sources of materials, including aggregate, cement, cementitious additives, curing, and bond-breaking materials.

- Physical properties of the aggregates, cement, cementitious additives, curing, and bond-breaking materials.

- Mix design

  - mix identification number.

  - aggregate gradation.

  - cement content.

  - water content.

  - cementitious materials content.

d.	Laboratory test results

  - compaction and strength testing procedures.

  - laboratory compaction characteristics (maximum dry density and optimum moisture content).

  - compressive strength at 7 days.

  - Wet-dry and/or freeze-thaw weight loss, if applicable.

No CTB material shall be placed until the submittal is accepted in writing by the Engineer.

During production, the Contractor shall submit batch tickets for each delivered load.

* * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * *

Insert the appropriate number of days for Contractor submittal of certified test reports for the proposed materials; 10 to 20 days is typical.

* * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * *

#### EQUIPMENT

All equipment necessary to mix, transport, place, compact, and finish the CTB material shall be furnished by the Contractor.  The equipment shall be inspected and approved by the Engineer at the job site prior to the start of construction operations.

304-4.1  MIXING.  The mixer shall be a batch or continuous-flow type stationary mixer and shall be equipped with calibrated metering and feeding devices that introduce the aggregate, cement, water, and cementitious additives (if used) into the mixer in the specified quantities.  If necessary, a screening device shall be used to remove oversized material greater than 2 in (51 mm) from the raw aggregate feed prior to mixing.

Free access to the plant must be provided at all times for inspection of the plant’s equipment and operation and for sampling the CTB mixture and its components, as deemed necessary by the Engineer.

304-4.2  HAULING.  The mixed CTB material shall be transported from the plant to the job site in trucks or other hauling equipment having beds that are smooth, clean, and tight.  Truck bed covers shall be provided and used to protect the CTB from rain.  CTB material that becomes wet during transport shall be subject to rejection.

304-4.3  PLACING.  CTB material shall be placed using a mechanical spreader or a machine capable of receiving, spreading, and shaping the mixture without segregation into a uniform layer or lift.  The equipment shall be equipped with a strike-off plate capable of being adjusted to the specified layer thickness.  It shall also be equipped with two end gates or cut off plates, so that the CTB may be spread in widths varying up to lane width.

304-4.4  COMPACTION.  Compaction of the CTB layer shall be accomplished using one or a combination of the following pieces of equipment:

- Tamping or grid roller.

- Steel-wheeled roller

- Vibratory roller.

- Pneumatic-tire roller.

- Vibrating plate compactor (for areas inaccessible to rollers).

The number, type, and weight of rollers and/or compactors shall be sufficient to compact the mixture to the required density.

304-4.5  FINISHING.  Final trimming of the compacted CTB to meet surface requirements shall be accomplished using a self-propelled grader or trimming machine, with a mold board cutting edge, which is at least 12 ft (3.7 m) wide and is automatically controlled by sensors in conjunction with an independent grade control from a taut stringline.  Stringline will be required on both sides of the sensor controls for the pilot lane.  For all other lanes, a single stringline on the outside and grade matching with previously completed adjacent lanes is permissible.

#### CONSTRUCTION METHODS

304-5.1  WEATHER LIMITATIONS.

304-5.1.1  Cold Weather.  The CTB material shall not be mixed or placed while the air temperature is below 40°F (4°C) or when conditions indicate that the temperature may fall below 35°F (2°C) within 24 hours.  The CTB shall not be placed on frozen surfaces.

304-5.1.1  Rain.  The CTB may not be placed when rainfall is occurring.  If an unexpected rain event occurs during placement, the layer should be quickly compacted.  CTB material that becomes wet by rain during transport or placement shall be evaluated by the Engineer, and may be subject to rejection.

304-5.2  PREPARATION OF UNDERLYING COURSE.  The underlying course shall be checked by the Engineer before placing and spreading operations are started, in order to ensure that it is free of any ruts, depressions, or bumps and is finished to the correct grade.  Any ruts or soft yielding places caused by improper drainage conditions, hauling, or any other cause, shall be corrected before the CTB mixture is placed thereon.  The underlying course shall be wetted in advance of placing the CTB layer.  The final prepared grade prior to placing the CTB should be in a firm and moist condition free of frost.  Use of chemicals to eliminate frost will not be permitted.

To ensure proper drainage, placement of the base shall begin along the centerline of the pavement on a crowned section or on the highest elevation contour of a pavement with variable cross slope.

304-5.3  GRADE CONTROL.  Grade control between the edges of the CTB shall be accomplished at intervals of 50 ft (15.2 m) or less on the longitudinal grade and at 25 ft (7.6 m) or less on the transverse grade.

304-5.4  HANDLING, MEASURING, AND BATCHING.  The continuous flow central plant site, layout, equipment, and provisions for transporting material shall assure a

continuous supply of material to the work.  Aggregate stockpiles shall be constructed in a manner that prevents segregation and intermixing of deleterious materials.

Aggregates that are segregated or mixed with earth or foreign material will not be accepted.

Continuous flow plants shall be equipped with feeders to proportion aggregates and bulk cement, by weight, automatically and accurately.  When bulk cement is used, the Contractor shall use a suitable method of handling the cement from weighing hopper to transporting container or into the batch itself for transportation to the mixer, such as a chute, boot or other device, to prevent loss of cement.  The device shall be arranged to provide positive assurance that the cement content specified is present in each batch.

304-5.5  MIXING.  Aggregate and cement may be proportioned either by weight or volume, and shall be mixed sufficiently to prevent the forming of cement balls when water is added.  The mixing time shall be that which is required to secure an intimate, uniform mixture of aggregate, cement, water, and pozzolan (if used).  The minimum mixing time will be based on the uniformity and consistency of the mixture.

304-5.6  PLACING.  The CTB mixture shall be deposited on the moistened subgrade or subbase and spread into a uniform layer of such width and thickness that, following compaction and trimming, conforms to the required grade and cross-section.  The Contractor may install the CTB layer in single or multiple compacted lifts; however, each compacted lift must be no greater than 6 in (152 mm) thick.  In multi-lift construction, the surface of the compacted lift shall be kept moist until covered with the next lift.  Successive lifts shall be placed and compacted so that the required total depth of the CTB layer is completed within 12 hours.

A single spreader may be used, provided it is capable of placing a uniform, full-depth layer of material across the full width of the base in one pass.  Otherwise, two or more spreaders will be required, and shall be operated so that spreading progresses along the full width of the base in a uniform manner.

304-5.7  COMPACTION.  Immediately upon completion of the spreading operations, the CTB material shall be thoroughly compacted using approved compaction equipment.  At the start of compaction, the moisture content shall be within 2 percentage points of the specified optimum moisture.

304-5.8  FINISHING.  Upon completion of compaction, the surface of the CTB layer shall be shaped to the specified lines, grades, and cross-section.  During the finishing process, the surface shall be kept moist by means of fog-type sprayers.  Compaction and finishing shall be done in such a manner as to produce a smooth, dense surface, free of ruts, cracks, ridges, and loose material.  All placement, compaction, and finishing operations shall be completed within 2 hours from the start of mixing.  Material not completed within the 2-hour time limit shall be removed and replaced at the Contractor’s expense.

CTB layer limits that extend beyond the edges of the new PCC surface course shall be rolled down or shaped in such a manner that the drainage is away from the new PCC surface course edge.

304-5.9  CONSTRUCTION JOINTS.  At the end of each day's construction, a transverse construction joint shall be formed that is a true vertical face (perpendicular to the centerline) and is free of loose material.

Longitudinal construction joints (parallel to the centerline) shall be formed to a consistent, well-defined near vertical edge that is free of loose material.  The longitudinal joints shall be located such that there is a 2-ft (0.6-m) minimum offset from planned joints in any overlying layer.

While forming construction joints, the Contractor shall make sure the material in the joint area is adequately compacted and that the joints are finished level and even with the remainder of the CTB layer.

304-5.10  CURING.  The compacted and finished CTB shall be cured with the approved curing agents as soon as possible, and in no case later than 2 hours after completion of the finishing operations.  The layer shall be kept moist using a moisture-retaining cover or a light application of water until the curing material is applied.

When asphalt emulsion is used as the curing agent, the entire surface of the CTB layer shall be uniformly sprayed with the emulsion at a rate of between 0.15 and 0.30 gal/yd2 (0.7 and 1.4 L/m2); the exact temperature and rate of application being that required to achieve complete and uniform coverage without runoff.  Should it be necessary for construction equipment or other traffic to use the asphalt-covered surface, sufficient sand blotter cover shall be applied to prevent pick-up.

When liquid membrane-forming curing compound is used as the curing agent, the entire surface of the CTB layer shall be uniformly sprayed with the compound at the rate of 1 gal (3.8 L) to not more than 200 ft2 (18.6 m2).  The rate of application shall be determined such that a uniform surface is obtained.  The spraying equipment shall be of the fully atomizing type equipped with a tank agitator.  The compound shall be thoroughly mixed with the pigment uniformly dispersed throughout the storage tank.  During application, the compound shall be stirred continuously by effective mechanical means.  Hand spraying of odd widths or shapes and CTB surfaces exposed by the removal of forms is permitted.

The curing seal shall be maintained and protected until the pavement is placed.  Should the surface of the finished CTB and/or the curing seal become damaged, additional curing material shall be applied at the time it is damaged or when the damage is first observed.

304-5.11  PROTECTION.  The Contractor shall protect the finished CTB against traffic.  Completed portions of the CTB layer can be opened immediately to low-speed traffic and to construction equipment, provided the curing material is not damaged and the CTB is sufficiently stable to resist permanent deformation.  Should the CTB be damaged, it shall be replaced using full-depth patches, and sprayed with the selected curing compound as described above.  The CTB shall also be protected from freezing at all times.

304-5.12  BOND-BREAKER.  When the CTB is to be placed directly beneath PCC, a bond-breaker selected by the Contractor shall be used.  The entire surface of the CTB shall be coated with a de-bonding compound applied in a quality sufficient to prevent bonding of the PCC pavement to the base course.  If an impervious membrane or asphalt emulsion is used as a curing material, additional applications of curing materials may be required. The Contractor shall be responsible for selecting the de-bonding compound and determining the necessary application rate. The de-bonding compound shall be approved by the Engineer prior to being incorporated into the work.

#### MATERIAL ACCEPTANCE

304-6.1  ACCEPTANCE SAMPLING AND TESTING.  All acceptance sampling and testing, with the exception of thickness determination, necessary to determine conformance with the requirements specified in this section will be performed by the Engineer.  The Contractor shall provide the required CTB samples during construction for acceptance testing purposes.  The samples shall be taken in the presence of the Engineer.

Testing organizations performing these tests shall meet the requirements of ASTM D 3666.  All test equipment in Contractor-furnished laboratories shall be calibrated by the testing organization prior to the start of operations.

The CTB layer shall be tested for density, thickness, grade, and surface tolerance on a lot basis, with a lot consisting of one of the following:

- One day’s production not to exceed [2,000 yd2 (1,675 m2)].

- A half day’s production, where a day’s production consists of [2,000 to 4,000 yd2 (1,675 to 3,350 m2)].

Each lot shall be divided into four (4) equal sublots.  Within each sublot, one (1) density test, one (1) thickness measurement, and continuous surface straightedge tests (surface tolerance testing) shall be performed, as described below.  Sampling locations shall be determined by the Engineer in accordance with the random sampling procedures contained in ASTM D 3665.

In the event that only three (3) sublots are produced, the three sublots shall constitute a complete lot.  If one (1) or two (2) sublots are produced for the same reason, they shall be incorporated into the next or previous lot, and the total number of sublots shall be used in the acceptance criteria calculation.

End-of-production sublots (i.e., sublots associated with the final placement of CTB for the project and are less than a complete lot) shall be handled as follows:

- Three (3) sublots shall constitute a lot.

- One (1) or two (2) sublots shall be incorporated into the previous lot.

304-6.1.1  Density Testing.  CTB samples shall be taken from each sublot and used to create laboratory test specimens representing the various sublots.  The specimens shall be compacted and tested for density and moisture content in accordance with ASTM D 558.  Using the density results for each sublot comprising a lot, an average density for the lot shall be determined, which will serve as the basis for acceptance of the lot with regard to density.

Within each sublot in the field, one (1) in-place density test shall be performed in accordance with ASTM D 1556, ASTM D 2167, or ASTM D 2922 and ASTM D 3017.  The location of the test shall be randomly selected in accordance with the procedures contained in ASTM D 3665.  The in-place density results for each sublot comprising the lot shall then be averaged and compared with the corresponding average lot density.  Acceptance criteria for CTB density are provided in paragraph 304-6.2.1.

304-6.1.2  Thickness Testing.  The CTB shall be tested for thickness using the same lot and sublot designations established for density testing.  After 3 days of curing, one (1) 4-in (102-mm) diameter core per sublot shall be obtained from a random location, as identified using the procedures contained in ASTM D 3665.  The thickness of each sampled core shall be determined using the caliper measurement procedures provided in ASTM C 174.  The average thickness for the lot shall be determined using the individual sublot core thicknesses.  Acceptance criteria for CTB thickness are provided in paragraph 304-6.2.2.  At all locations where cores have been drilled, the resulting core holes shall be filled by the Contractor with CTB, HMA, or non-shrink grout.

304-6.1.3 Grade Testing.  The elevations of the finished CTB shall be surveyed every 25 ft (7.6 m) on both sides of the CTB lane as soon as it has hardened sufficiently.  Acceptance criteria for CTB grade are provided in paragraph 306-6.2.3.

304-6.1.4  Surface Tolerance Testing.  As soon as the CTB has hardened sufficiently, it shall be tested for surface tolerance with a 16-ft (4.9-m) straightedge or other approved measuring device.

304-6.2  ACCEPTANCE CRITERIA.  Acceptance of CTB will be based on density, thickness, grade, and surface tolerance, as described in the paragraphs below.

304-6.2.1  Density Requirements.  With respect to density, each lot of compacted material will be accepted without adjustment if the average in-place density of the lot is equal to or greater than 98 percent of the average density determined for the lot.  Each lot of compacted CTB shall be accepted and payment adjusted in accordance with Table 3.

Table 3.  Sliding pay scale factors for density.

| Average Dry Density (%) | Payment (%) |
| --- | --- |
| 98.0 and greater | 100 |
| 97.0 - 97.9 | 95 |
| 96.0 - 96.9 | 90 |
| 95.0 - 95.9 | 75 |
| Less than 95.0 | Reject |

If the average density is below 95 percent, the lot will be rejected and shall be removed and replaced at the Contractor’s expense.  In multi-layer construction, density shall be tested for each lift, and all lifts within a rejected lot shall be removed and replaced.  No payment shall be made for removed lifts.  Replacement lifts shall be paid in accordance with this section.

304-6.2.2  Thickness Requirements.  The completed thickness shall be as shown on the plans.  When the average lot thickness is not deficient by more than ½ in (12.5 mm) from the plan thickness, full payment shall be made.  If the average lot thickness is deficient by more than 1 in (25.4 mm), it shall be removed and replaced at the Contractor’s expense.  When such measurement is deficient by more than ½ in (12.5 mm) but less than 1 in (25.4 mm) from the plan thickness, one additional core shall be taken at random from each sublot within the lot.  The thickness of these additional cores shall be determined as indicated in paragraph 304-6.1.2.  A new average lot thickness shall be recomputed based on these additional cores and the original cores taken from each sublot.  If the recomputed average lot thickness is not deficient by more than ½ in (12.5 mm) from the plan thickness, full payment shall be made.  If the average lot thickness is deficient by more than ½ in (12.5 mm) from the plan thickness, the entire lot shall be removed and replaced at the Contractor's expense or shall be permitted to remain in-place at an adjusted payment of 75 percent of the contract unit price.

When the measured thickness is more than that indicated on the plans, it will be considered as conforming to the requirements, provided the surface of the completed CTB layer is within the established grade and surface tolerance requirements.

304-6.2.3  Grade Requirements.  When the completed surface is higher than ½ in (12.5 mm) above the grade shown in the plans, the surface shall be trimmed, at the Contractor’s expense, with an approved grinding machine to an elevation that falls within a tolerance of ¼ in (6 mm) or less.

304-6.2.4  Surface Tolerance Requirements.  The finished surface shall not vary more than ⅜ in (9.5 mm) when tested with a 16-ft (4.9-m) straightedge applied parallel with, or at right angles to, the centerline of the CTB area.  Areas in the CTB showing high spots greater than ⅜ in (9.5 mm) over 16 ft (4.9 m) shall be marked and immediately trimmed with an approved grinding machine.  Such trimming shall be at the Contractor’s expense.

#### METHOD OF MEASUREMENT

304-7.1  CEMENT-TREATED BASE COURSE.  The quantity of cement-treated base course to be paid for will be determined by measurement of the number of [yd2 (m2)] of CTB actually constructed and accepted by the Engineer as complying with the plans and specifications.

#### BASIS OF PAYMENT

304-8.1  CEMENT-TREATED BASE COURSE.  Payment shall be made at the contract unit price per [yd2 (m2)] for cement-treated base course.  This price shall be full compensation for furnishing all materials, including cement; for all preparation, manipulation, placing, and curing of these materials; and for all labor, equipment, tools, and incidentals necessary to complete the item.

Each lot of CTB material will be accepted for density at the full contract price adjusted in accordance with Table 3 in paragraph 304-6.2.1.

Payment will be made for cement-treated base course--per [yd2 (m2)].

#### TESTING REQUIREMENTS

ASTM C 88		Soundness of Aggregates by Use of Sodium Sulfate or

Magnesium Sulfate

ASTM C 131	Resistance to Degradation of Small-Size Coarse Aggregate

by Abrasion and Impact in the Los Angeles Machine

ASTM C 136	Sieve or Screen Analysis of Fine and Coarse Aggregate

ASTM C 174	Measuring Thickness of Concrete Elements Using Drilled

Concrete Cores

ASTM D 75		Sampling Aggregates

ASTM D 558	Moisture-Density Relations of Soil-Cement Mixtures

ASTM D 559	Test Methods for Wetting & Drying Compacted Soil Cement

Mixtures

ASTM D 560	Freezing-and-Thawing Tests of Compacted Soil-Cement Mixtures

ASTM D 1556	Density of Soil in Place by the Sand-Cone Method

ASTM D 1633	Compressive Strength of Molded Soil-Cement Cylinders

ASTM D 2167	Density of Soil in Place by the Rubber-Balloon Method

ASTM D 2922	Density of Soil and Soil-Aggregate in Place by Nuclear Methods

ASTM D 3017	Water Content of Soil and Rock in Place by Nuclear Methods

ASTM D 3665	Random Sampling of Paving Materials

ASTM D 3666	Minimum Requirements for Agencies Testing and Inspecting

Road and Paving Materials

ASTM D 4318	Liquid Limit, Plastic Limit, and Plasticity Index of Soils

AASHTO T 26	Quality of Water to be Used in Concrete

#### MATERIAL REQUIREMENTS

ASTM C 150	Portland Cement

ASTM C 309	Liquid Membrane-Forming Compounds for Curing Concrete

ASTM C 595	Blended Hydraulic Cements

ASTM C 618	Coal Fly Ash and Raw or Calcined Natural Pozzolan for Use as a

Mineral Admixture in Concrete

ASTM C 989	Ground Granulated Blast-Furnace Slag for Use in Concrete

and Mortars

ASTM D 977	Emulsified Asphalt

ASTM D 2397	Cationic Emulsified Asphalt

End P-304

### ITEM P-306  ECONOCRETE BASE COURSE

#### DESCRIPTION

306-1.1  This item shall consist of a subbase material, herein termed econocrete, that is  composed of aggregate and cement uniformly blended together and mixed with water.  The mixture may also include approved cementitious additives, in the form of fly ash or slag, and chemical admixtures.  The mixed material shall be spread, shaped, and consolidated using concrete paving equipment in accordance with these specifications and in conformity to the lines, grades, dimensions, and typical cross-sections shown on the plans.

#### MATERIALS

306-2.1  AGGREGATE.  The coarse aggregate fraction shall be crushed stone, crushed or uncrushed gravel, crushed and adequately seasoned, air-cooled, iron blast furnace slag, crushed recycled concrete, or a combination thereof.  The fine aggregate fraction may be part of the natural aggregate blend as obtained from the borrow source or it may be natural sand that is added at the time of mixing.

The aggregate shall consist of hard, durable particles, free from an excess of flat, elongated, soft, or disintegrated pieces, or objectionable matter (e.g., roots, sod, weeds, organic impurities, etc.).  A flat particle is one having a ratio of width to thickness greater than five; an elongated particle is one having a ratio of length to width greater than five.

* * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * *

The Engineer should specify limits for deleterious materials using guidance contained in ASTM C 33.

* * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * *

The design aggregate blend shall conform to one of the gradations shown in Table 1, when tested in accordance with ASTM C 136.

Table 1.  Aggregate gradation for econocrete.

| Sieve Size (square openings) | Percentage by Weight Passing Sieves |
| --- | --- |
|  | 1½ -in (37.5-mm) Maximum | 1-in (25-mm) Maximum |
| 2 in (51 mm) 1½ in (37.5 mm) 1 in (25 mm) ¾ in (19 mm) No. 4 (4.75 mm) No. 40 (425 µm) No. 200 (75 µm) | -- 100 70 - 95 55 - 85 30 - 60 10 - 30 0 - 15 | -- -- 100 70 - 100 35 - 65 15 - 30 0 – 15 |

306-2.2  CEMENT.  Cement shall conform to the requirements of ASTM [    ].

* * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * *

The Engineer shall specify ASTM C 150 Type I, II, III, IV, or V or ASTM C 595 Type IS, IS-A, IP, IP-A, P, or PA.   Type II cement shall be specified in areas with a history of sulfate reaction with the selected aggregate.

* * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * *

306-2.3  CEMENTITIOUS ADDITIVES.  Pozzolanic and ground granulated blast furnace (GGBF) slag may be added to the econocrete mix.  If used, each material must meet the following requirements:

- Pozzolan.  Pozzolanic materials must meet the requirements of ASTM C 618, Class F Flyash.

- Ground Granulated Blast Furnace  Slag (Slag Cement).  Slag shall conform to ASTM C 989, Grade 80, 100 or 120.

306-2.4  CHEMICAL ADMIXTURES.    The Contractor shall submit certificates indicating that the material to be furnished meets all the requirements listed below.  In addition, the Engineer may require the Contractor to submit complete test data showing that the material to be furnished meets all the requirements of the cited specification.

- Air-Entraining Admixtures.  Air-entraining admixtures shall meet the requirements of ASTM C 260.

- Water-Reducing Admixtures.  Water-reducing, set-controlling admixtures shall meet the requirements of ASTM C 494, Type A, water-reducing or Type D, water-reducing and retarding.  Water-reducing admixtures shall be added at the mixer separately from air-entraining admixtures in accordance with the manufacturer's printed instructions.  The air entrainment agent and the water-reducing admixture shall be compatible.

306-2.5  WATER.  Water used in mixing or curing shall be clean and free of oil, salt, acid, alkali, sugar, vegetable, or other deleterious substances injurious to the finished product.  Water will be tested in accordance with the requirements of AASHTO T 26.  Water known to be of potable quality may be used without testing.

306-2.6  CURING MATERIALS.  For curing econocrete, use white-pigmented, liquid membrane-forming compound conforming to ASTM C 309, Type 2, Class A or Class B (wax-based) or Asphalt emulsion conforming to the requirements of ASTM D 977, Type SS-1h..

* * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * *

The Engineer may add additional curing materials  Modify the Bond Breaker paragraph accordingly.

* * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * *

#### COMPOSITION OF MIXTURE

306-3.1  MIX DESIGN.  The econocrete mix design shall be based on trial batch results conducted in the laboratory.  The econocrete shall be designed to meet the criteria in this section.

306-3.1.1  Compressive Strength.  Compressive strength shall not be less than 500 psi (3,445 kPa) nor greater than 800 psi (5,516 kPa) at 7 days.  3-day and 7-day strengths shall be taken as the average of two compressive strength test results.  All compressive strength specimens shall be prepared and tested in accordance with ASTM C 192 and ASTM C 39, respectively.

If the 3-day strength is greater than 500 psi (3,447 kPa), the Contractor shall construct  transverse joints in the econocrete layer in accordance with paragraph 306-5.10.2.

* * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * *

In locations subject to freeze-thaw cycles, insert the following “The freeze-thaw weight loss shall not exceed 14 percent when tested in accordance with ASTM D 560.”

* * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * *

If there is a change in aggregate sources, type of cement used, or pozzolanic materials, a new mix design must be submitted.

306-3.1.2  Air Content.  The percentage of air entrainment shall be 6 percent, plus or minus 1/2 percent.  Air content shall be determined by testing in accordance with ASTM C 231 for gravel and stone coarse aggregate and ASTM C 173 for slag and other highly porous coarse aggregate.

306-3.2  SUBMITTALS.  At least  [    ] days prior to the placement of the econocrete, the Contractor shall submit certified test reports to the Engineer for those materials proposed for use during construction, as well as the mix design information for the econocrete material.  Tests older than 6 months shall not be used.  The certification shall show the appropriate ASTM or AASHTO specifications or tests for the material, the name of the company performing the tests, the date of the tests, the test results, and a statement that the material did or did not comply with the applicable specifications.  The submittal package shall include the following:

- Sources of materials, including aggregate, cement, admixtures, and curing and bond breaking materials.

- Physical properties of the aggregates, cement, admixtures, curing and bond breaking materials.

- Mix design.

- mix identification number.

- weight of saturated surface-dry aggregates (fine and coarse).

- combined aggregate gradation.

- cement factor.

- water content.

- water-cementitious material ratio (by weight).

- volume of admixtures and yield for one cubic yard (cubic meter) of econocrete.

- Laboratory test results.

- slump.

- air content.

- compressive strength at 3, 7, and 28 days (average values).

- wet/dry and/or freeze-thaw weight loss (when applicable).

In addition, where applicable, the Contractor shall submit for approval by the Engineer a jointing plan for transverse joints in the econocrete layer.

During production, the Contractor shall submit batch tickets for each delivered load.

* * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * *

Insert the appropriate number of days for Contractor submittal of the certified test reports and the mix design; 15 to 30 days is typical.

* * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * *

#### EQUIPMENT

306-4.1  All equipment necessary to mix, transport, place, compact, and finish the econocrete material shall be furnished by the Contractor.  The equipment shall be subject to inspection and approval by the Engineer.

306-4.2  MIXING.  Econocrete may be mixed in a stationary mixer, either at a central batch plant or at the site, or in a truck mixer.  The mixer type and capacity shall be inspected and approved by the Engineer before production begins.  Each mixer shall have attached in a prominent place a manufacturer's nameplate showing the capacity of the drum in terms of volume of mixed concrete and the speed of rotation of the mixing drum or blades.

306-4.2.1  Stationary Plant Mixer.  The batch plant and equipment shall conform to the requirements of ASTM C 94.  Unrestricted access to the plant must be provided to the Engineer at all times for inspection of the plant’s equipment and operation and for sampling the econocrete mixture and its components.

The mixers shall be examined daily for changes in condition due to accumulation of hard concrete or mortar or wear of blades.

306-4.2.2  Truck Mixers.  Truck mixers used for mixing econocrete shall conform to the requirements of ASTM C 94.  Econocrete may be entirely mixed in a truck mixer or partially mixed in a stationary mixer with mixing completed in a truck mixer.  Truck mixers shall be equipped with an accurate continuous registering electronically or mechanically activated revolution counter, by which the number of drum revolutions may be verified.

306-4.3  HAULING.  Mixed econocrete shall be hauled from the stationary plant to the job site in a truck agitator, a truck mixer operating at agitating speed, or a non-agitating truck.  All equipment shall conform to the requirements of ASTM C 94.  When truck mixers are used to mix econocrete, they may be transported to the job site in the same truck operating at agitating speeds, truck agitators, or a non-agitating truck.  The bodies of non-agitating trucks shall be smooth, metal containers and shall be capable of discharging the concrete at a satisfactory controlled rate without segregation.

306-4.4  PLACING AND FINISHING.

306-4.1  Forms.  Straight side forms shall be made of steel and shall be furnished in sections not less than 10 ft (3.1 m) in length.  Forms shall have a depth equal to the pavement thickness at the edge.  Flexible or curved forms of proper radius shall be used for curves of 100-ft (31-m) radius or less.  Forms shall be provided with adequate devices for secure settings so that when in place they will withstand, without visible spring or settlement, the impact and vibration of the consolidating and finishing equipment.  Forms with battered top surfaces and bent, twisted or broken forms shall not be used.  Built-up forms shall not be used, except as approved by the Engineer.

The top face of the form shall not vary from a true plane more than ⅛ in (3 mm) in 10 ft (3.1 m), and the upstanding leg shall not vary more than ¼ in (6 mm).  The forms shall contain provisions for locking the ends of abutting sections together tightly for secure setting.  Wood forms may be used under special conditions, when accepted by the Engineer.

306-4.4.2  Pavers.  Econocrete can be placed using fixed forms or slip-form pavers.  The paver shall be fully energized, self-propelled and capable of spreading, consolidating, and finishing the econocrete material, true to grade, tolerances, and cross sections.  The paver shall be capable of finishing the surface so that hand finishing is not required.  The paver shall be of sufficient weight and power to construct the maximum specified concrete paving lane width, at adequate forward speed, without transverse, longitudinal or vertical instability or without displacement.  The slip-form paver shall be equipped with electronic or hydraulic horizontal and vertical control devises utilizing guide wires or stringlines on both sides of the machine.  Slope control will not be allowed.

- Concrete Pavers.  Concrete pavers are approved as paver-finishing machines for econocrete, providing they are capable of handling the amount of econocrete required for the full-lane width specified, and consolidating the econocrete full depth.  A concrete paver is a power-driven machine with augers, strike-off and tamper bars ahead of a pan screed, with at least one trailing oscillating screed or belt finisher.

- Bridge Deck Pavers.  Bridge deck pavers are approved as paver-finishing machines for econocrete, providing they are capable of handling the amount of econocrete required for the full-lane width specified, and consolidating the econocrete full depth.  A bridge deck paver is an automatic truss paving machine, with paving carriage that strikes off, vibrates, paves, and textures the econocrete with augers, internal vibration, paving rollers, and drag pan.

* * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * *

Econocrete is a weak concrete mix.  As such, it should be placed with pavers suitable for paving concrete pavements.  Rotating pipe and tube floats are not suitable for this type of pavement.

* * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * *

306-4.5  CONSOLIDATION.  For side-form construction, vibrators may be either the surface pan type for pavements less than 8 in (203 mm) thick or the internal type with either immersed tube or multiple spuds for the full width of the slab.  They may be attached to the spreader or the finishing machine, or they may be mounted on a separate carriage.  They shall not come in contact with the joint, subgrade, or side forms.

For slip-form construction, the paver shall vibrate the econocrete for the full width and depth of the strip of pavement being placed.  Vibration shall be accomplished by internal vibrators.

The number, spacing, frequency, and eccentric weights of vibrators shall be provided as necessary to achieve acceptable consolidation without segregation and finishing quality.  Adequate power to operate all vibrators at the weight and frequency required for a satisfactory finish shall be available on the paver.  The internal vibrators may be supplemented by vibrating screeds operating on the surface of the econocrete.  The Contractor shall constantly monitor the frequency of each of the individual vibrators using electronic means and shall provide constant monitoring of the consolidation process to avoid honeycombing or segregation.  Areas that are visually determined to be honeycombed or over-consolidated shall be corrected at the Contractor’s expense.

The vibrators and tamping elements shall be automatically controlled so that they stop operation as forward motion ceases.  Any override switch shall be of the spring-loaded, momentary-contact type.

Hand held vibrators may be used in irregular areas.

306-4.6  JOINTING.  The Contractor shall provide sawing equipment adequate in number of units and power to produce contraction or construction joints of the required dimensions as shown on the plans.  The Contractor shall provide at least one standby saw in good working order and a supply of saw blades at the site of the work at all times during sawing operations.

#### CONSTRUCTION METHODS

306-5.1  WEATHER LIMITATIONS.

306-5.1.1  Cold Weather.  Unless authorized by the Engineer, the temperature of the mixed econocrete shall not be less than 50°F (10°C) at the time of placement.  In addition, the econocrete shall not be placed when the ambient temperature is below 40°F (4°C) or when conditions indicate that the temperature may fall below 35°F (2°C) within 24 hours.  Under no circumstances shall the econocrete be placed on frozen underlying courses or mixed when the aggregate is frozen.

When mixing and placing is authorized during cold weather, the Engineer may require the water and/or the aggregates to be heated to not less than 70°F (20°C) nor more than 150°F (66°C).  The aggregates may be heated by either steam or dry heat prior to being placed in the mixer.  The apparatus used shall heat the mass uniformly and shall be arranged to preclude the possible occurrence of overheated areas which might be detrimental to the materials.

306-5.1.2  Hot Weather.  To prevent rapid drying of newly constructed econocrete, the econocrete temperature from initial mixing through final cure shall not exceed 90°F (32°C).  The aggregates and/or mixing water shall be cooled as necessary to maintain the econocrete temperature at or not more than the specified maximum.  Ice or ice water may be substituted for the mixing water for this purpose.

In addition, during periods of warm weather when the maximum daily air temperature exceeds 85°F (30°C), the forms and/or the underlying material shall be sprinkled with water immediately before placing the econocrete.

306-5.1.3  Rain.  All mixing and batching operations should be halted during rain showers and any plastic econocrete placed should be covered immediately.  The econocrete shall be kept covered with plastic sheeting or other waterproof material until such time that the rain does not make any surface indentation on the econocrete layer.    Areas damaged by rain shall be refinished or replaced.

306-5.2  FORM SETTING.  Forms shall be set sufficiently in advance of the econocrete placement to ensure continuous paving operation.  After the forms have been set to correct grade, the grade shall be thoroughly tamped, either mechanically or by hand, at both the inside and outside edges of the base of the forms.  Forms shall be staked into place with not less than 3 pins for each 10-ft (3.1-m) section.  A pin shall be placed at each side of every joint.

Form sections shall be tightly locked and shall be free from play or movement in any direction.  The forms shall not deviate from true line by more than ¼ in (6 mm) at any joint.  Forms shall be so set that they will withstand, without visible spring or settlement, the impact and vibration of the consolidating and finishing equipment.  Forms shall be cleaned and oiled prior to the placing of econocrete.

The alignment and grade elevations of the forms shall be checked and corrections made by the Contractor immediately before placing the econocrete.  When any form has been disturbed or any grade has become unstable, the form shall be reset and rechecked.

306-5.3  PREPARATION OF UNDERLYING COURSE.  The underlying course shall be checked by the Engineer before placing and spreading operations are started, in order to ensure that it is free of any ruts, depressions, or bumps and is finished to the correct grade.  Any ruts or soft yielding places in the underlying course caused by improper drainage conditions, hauling, or any other cause, shall be corrected at the Contractor’s expense before the econocrete mixture is placed thereon.  The underlying course should be wetted down in advance of placing the econocrete to ensure a firm, moist condition at the time of econocrete placement.  The underlying course shall be protected from frost.  Usage of chemicals to eliminate frost is not permissible.

306-5.4  GRADE CONTROL.  Grade control between the edges of the pavement shall be accomplished at intervals of 50 ft (15.3 m) or less on the longitudinal grade and at 25 ft (7.6 m) or less on the transverse grade.  To protect the underlying course and ensure proper drainage, the econocrete paving shall begin along the centerline of the pavement on a crowned section or on the greatest contour elevation of a pavement with variable cross slope.

306-5.5  HANDLING, MEASURING, AND BATCHING MATERIAL.  The batch plant site, layout, equipment, and provisions for transporting material shall assure a

continuous supply of material to the work.  Stockpiles shall be constructed in a manner that prevents segregation and intermixing of deleterious materials.

Aggregates that have become segregated or mixed with earth or foreign material shall not be used.  All aggregates produced or handled by hydraulic methods, and washed aggregates, shall be stockpiled or binned for draining at least 12 hours before being batched.  Rail shipments requiring more than 12 hours transit will be accepted as adequate binning only if the car bodies permit free drainage.

Batching plants shall be equipped to proportion aggregates and bulk cement, by weight, automatically using interlocked proportioning devised of an approved type.  When bulk cement is used, the Contractor shall use a suitable method of handling the cement from weighing hopper to transporting container or into the batch itself for transportation to the mixer, such as a chute, boot or other device approved by the Engineer, to prevent loss of cement.  The device shall be arranged to provide positive assurance that the required cement content is present in each batch.

306-5.6  MIXING.  All econocrete shall be mixed and delivered to the site in accordance with the requirements of ASTM C 94.  The mixing time should be adequate to produce econocrete that is uniform in appearance, with all ingredients evenly distributed.  Mixing time shall be measured from the time all materials are emptied into the drum (provided all the water is added before one-fourth the preset mixing time has elapsed) and continues until the time the discharge chute is opened to deliver the econocrete.

If mixing in a plant, the mixing time shall not be less than 50 nor greater than 90 seconds.  If mixing in a truck, the mixing time shall not be less than 70 nor more than 125 truck-drum revolutions at a mixing speed of not less than 6 nor more than 18 truck-drum revolutions per minute.

Retempering econocrete by adding water or by other means will not be permitted, except when econocrete is delivered in truck mixers.  With truck mixers, additional water may be added to the batch materials and additional mixing performed to allow proper placement of the material, provided (a) the addition of water is performed within 45 minutes after the initial mixing operations and (b) the water/cementitious ratio specified in the mix design is not exceeded.

306-5.7  HAULING.  The elapsed time from the addition of cementitious material to the mix until the econocrete is deposited in place at the work site shall not exceed 45 minutes when the concrete is hauled in nonagitating trucks, nor 90 minutes when it is hauled in truck mixers or truck agitators.

306-5.8  PLACING, CONSOLIDATING, AND FINISHING.  Prior to placement of the econocrete layer, the prepared underlying course shall be well moistened with water, without saturating, in order to prevent rapid loss of moisture from the econocrete.  In cold weather, the underlying course shall be protected so that it will be entirely free of frost when econocrete is placed.

The Contractor has the option of side- (fixed-) form or slip-form paving.  Under both techniques, the hauled econocrete material shall be discharged onto the prepared underlying course such that segregation of the mix is minimized and minimum handling of the mix is needed.  Placement of the econocrete material shall be continuous between construction joints.  Workers shall not be allowed to walk in the freshly mixed econocrete with boots or shoes coated with earth or debris.

Econocrete shall not be mixed, placed, or finished when the natural light is insufficient, unless an adequate artificial lighting system is provided.

306-5.8.1  Side-Form Construction.  For side-form placement, the Contractor shall verify the elevations of the fixed forms such that the thickness and finished grade of the econocrete layer will be in accordance with the requirements of the project plans and specifications.  The econocrete shall be spread uniformly between the forms, immediately after it is placed using a spreading machine.  Necessary hand spreading shall be done with shovels, not rakes.

The spreading shall be followed immediately by thorough consolidation using vibrating screeds or spud vibrators.  Vibrators may be external or internal type, depending on the thickness of the econocrete layer.  The surface vibrators may be attached to the spreader or they may be mounted on a separate carriage.  They shall not come in contact with the joint, subgrade, or side forms.  When spud vibrators are used, the econocrete shall be thoroughly consolidated against and along the faces of all forms and previously placed econocrete.  Vibrators shall not be permitted to come in contact with a joint assembly, the grade, or a side form.  In no case shall the vibrator be operated longer than 20 seconds in any one location, nor shall the vibrators be used to move the econocrete.

Hand finishing will not be permitted except in areas where the mechanical finisher cannot operate.

306-5.8.2  Slip-Form Construction.  For slip-form construction, the Contractor shall verify the elevations of the guide wires controlling slip-form pavers such that the thickness and finished grade of the econocrete will be in accordance with the requirements of the project plans and specifications.  The slip-form paver should spread, consolidate, and shape the freshly placed econocrete in one complete pass of the machine.  The machine shall vibrate and finish the econocrete for the full width and depth of the layer.

306-5.9  Final Finishing.  Final finishing shall be accomplished while the econocrete is still in the plastic state.  Limited surface refinishing by hand is acceptable to meet the grade and surface tolerance established in paragraphs 306-6.2.3 and 306-6.2.4, after strike off and consolidation.

If the overlying layer is to be PCC pavement, the surface of the econocrete shall not be textured.  If the overlying layer is to be HMA pavement, and if the bond between the HMA layer and the econocrete is considered important for pavement performance, tining or scarifying the surface to provide a coarse texture may be permitted.

306-5.10  JOINTS.  Joints shall be constructed as shown on the plans.

306-5.10.1  Construction Joints.  Locate all longitudinal and transverse construction joints as shown on the plans.  If longitudinal joints are not shown, locate longitudinal joints within 6 in (152 mm) from planned joints in the PCC to be placed over the econocrete.

306-5.10.2  Contraction Joints.  If required by paragraph306-3.1.1or if shown on the plans, transverse contraction joints shall be constructed by sawing the hardened econocrete to a depth of at least one-third the thickness of the econocrete base.  These joints shall match within 3 in (76 mm) the planned joints of the overlying concrete surface.

* * * * * * * * * * * * * * * * * * *  * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * *

The Engineer should include a note or detail on the plans when joints are required due to excessive strength or otherwise.

* * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * ** * * * * * * * * * * * * * * * * * * * * * * * *

306-5.10.3  Concrete Saws.  When sawing of joints are specified, the Contractor shall provide sawing equipment adequate in number of units and power to complete the sawing to the required dimensions and at the required rate.  The Contractor shall provide at least one standby saw in good working order.  An ample supply of saw blades shall be maintained at the site of the work at all times during sawing operations. The Contractor shall provide adequate artificial lighting facilities for night sawing. All of this equipment shall be on the job both before and at all times during econocrete placement.

306-5.11  CURING.  Immediately after the finishing operations are complete and within 2 hours of placement of the econocrete, the entire surface and edges of the newly placed econocrete shall be sprayed uniformly with white pigmented, liquid membrane forming curing compound.  The layer should be kept moist using a moisture-retaining cover or a light application of water until the curing material is applied.  The curing compound shall not be applied during rainfall.

* * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * *

Excessive delays in applying the curing compound can result in uncontrolled shrinkage cracking, which can reflect into the overlying pavement over time.

* * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * *

The curing material shall be applied using mechanical sprayers under pressure at the rate of 1 gal (3.8 L) to not more than 200 ft2 (18.6 m2).  The spraying equipment shall be of the fully atomizing type equipped with a tank agitator.  At the time of use, the compound in the tank shall be in a thoroughly mixed condition with the pigment uniformly distributed throughout the vehicle.  During application the compound shall be stirred continuously by mechanical means.

Hand spraying of odd widths or shapes and econocrete surfaces exposed by the removal of forms is permitted.

Should the film of curing material become damaged from any cause, including sawing operations, within the required 28-day curing period or until the overlying course is constructed, the damaged portions shall be repaired immediately with additional compound or other approved means as quickly as practical.

Edges of the econocrete layer shall be sprayed with curing compound immediately following placement with slip-form pavers or when side-forms are removed.

306-5.11.1  Curing in Cold Weather.  The econocrete shall be maintained at a temperature of at least 50°F (10°C) for a period of 72 hours after placing and at a temperature above freezing for the remainder of the curing time.  The Contractor shall be responsible for the quality and strength of the econocrete placed during cold weather, and any econocrete injured by frost action shall be removed and replaced at the Contractor's expense.

306-5.11.2  Curing in Hot Weather.  When econocrete is being placed and the air temperature may be expected to rise above 90°F (32°C) shortly after placement, the econocrete layer should be cured as quickly as possible to allow curing without the formation of excessive shrinkage cracks.

306-5.12  PROTECTION.  The Contractor shall protect the pavement and its appurtenances against both public traffic and traffic caused by the Contractor’s employees and agents.  The Engineer shall decide when the pavement shall be opened to traffic.  Traffic shall not be allowed on the pavement until test specimens molded and cured in accordance with ASTM C 31 have attained a compressive strength of 350 psi (2,413 kPa) when tested by ASTM C 39.  The econocrete surface shall be protected from foot and vehicular traffic and other sources of abrasion until such a time.  During this time, the econocrete layer shall be protected from injurious action by sun, rain, flowing water, frost, or mechanical injury.  After this period, construction traffic to place the overlying layers may be allowed.

306-5.13  BOND-BREAKER.  When the econocrete is to be placed directly beneath PCC pavement, a bond-breaker shall be used.  The entire surface of the econoncrete shall be coated with a de-bonding compound applied in a quality sufficient to prevent bonding of the PCC pavement to the econocrete.  If an impervious membrane or asphalt emulsion is used as a curing material, additional applications of curing materials may be required. The Contractor shall be responsible for selecting the de-bonding compound and determining the necessary application rate. The de-bonding compound shall be approved by the Engineer prior to being incorporated into the work. This application shall be made at least 8 hours and not more than 24 hours prior to beginning the placement of the PCC pavement.  The rate of application shall be the same as that specified for the curing application.  After application of the bond-breaker coat, traffic will be limited to that required for the placement of the overlying pavement layer.

#### MATERIAL ACCEPTANCE

306-6.1  ACCEPTANCE SAMPLING AND TESTING.  All acceptance sampling and

testing, with the exception of coring for thickness determination, necessary to determine conformance with the requirements specified in this section will be performed by the Engineer.  The Contractor shall provide the required econocrete samples during construction for acceptance testing purposes.  The samples shall be taken in the presence of the Engineer.

The econocrete layer shall be tested for air content, strength, thickness, grade, and surface tolerance.  Sampling and testing for air shall be as specified in paragraph 306-6.1.1.  Sampling and testing for strength, thickness, grade, and surface tolerance shall be on a lot basis, with a lot consisting of one of the following:

- One day’s production not to exceed 2,000 yd2 (1,675 m2).

- A half day’s production, where a day’s production is expected to consist of between 2,000 and 4,000 yd2 (1,675 and 3,350 m2).

Each lot will be divided into four equal sublots.  In the event that only three (3) sublots are produced, the three sublots shall constitute a complete lot.  If, only one (1) or two (2) sublots are produced, they shall be incorporated into the next lot, and the total number of sublots shall be used in the acceptance plan calculation.

End-of-production sublots (i.e., sublots associated with the final placement of econocrete for the project and are less than a complete lot) shall be handled as:

- Three (3) sublots shall constitute a lot.

- One (1) or (2) sublots shall be incorporated into the previous lot.

306-6.1.1  Air Content Testing.  Air content tests shall be performed on the first three truckloads of econocrete produced at the start of operations each day and the first three truckloads produced after any scheduled or non-scheduled shutdown.  Additional tests shall be performed each time a sample is taken for a strength test and when requested by the Engineer.

Air content tests shall be made in accordance with ASTM C 231.  Air content test results shall be between 4 and 8 percent.

If the first test on a truckload of econocrete is not within the specification limits, a second test on the same truckload shall be made.  If the second test is within the specification limits, the econocrete will be accepted with respect to entrained air content.  If the second test is not within the specification limits, the truckload shall be rejected.

306-6.1.2  Compressive Strength Testing.  One sample of freshly delivered econocrete shall be taken from each sublot for compressive strength testing.  The econocrete shall be sampled in accordance with ASTM C 172.  Sampling locations shall be determined in accordance with the random sampling procedures contained in ASTM D 3665.

At least two (2) test cylinders shall be made from each sample in accordance with ASTM C 31.  The 7-day compressive strength of each cylinder shall be determined in accordance with ASTM C 39.

* * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * *

Since the strength level of econocrete at an early age is considerably lower than PCC, special care is required in handling test specimens.

* * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * * *

The Contractor shall provide adequate facilities for the initial curing of cylinders.  During the 24 hours after molding, the temperature immediately adjacent to the specimens must be maintained in the range of 60 to 80°F (16 to 27°C), and loss of moisture from the specimens must be prevented.  The specimens may be stored in tightly constructed wooden boxes, damp sand pits, temporary buildings at construction sites, under wet burlap in favorable weather or in heavyweight closed plastic bags, or use other suitable methods, provided the temperature and moisture loss requirements are met.

The compressive strength for each sublot shall be computed by averaging the 7-day compressive strengths of the two test cylinders representing that sublot.  The compressive strength of the lot shall be the average compressive strength of the individual sublots comprising the lot.

Specimens that are noticeably defective shall not be considered in the determination of the strength.  If the test specimens fail to conform to the requirements for strength, the Engineer shall request changes in the econocrete mixture to increase the strength to meet the requirements.

If the maximum 7-day compressive strength values exceed the maximum strength requirements when evaluated in accordance with paragraph 306-6-2.1, the Contractor shall propose a jointing plan for approval by the Engineer.

306-6.1.3  Thickness Testing.  After the econocrete base has cured for 3 days, one (1) 4-in (102-mm) diameter core per sublot shall be obtained from a random location, as identified using the procedures contained in ASTM D 3665.  The thickness of each sampled core shall be determined using the caliper measurement procedures provided by ASTM C 174.  The average thickness for the lot shall be determined using the individual sublot core thicknesses.  Acceptance criteria for econocrete thickness are provided in paragraph 306-6.2.2.

When such measurement is deficient more than ½ in (12.5 mm) and not more than 1 in (25.4 mm) from the plan thickness, two additional cores shall be taken at random and used in determining the average thickness for that lot.  The thickness of the cores shall be determined by average caliper measurement of cores tested in accordance with ASTM C 174.

At all locations where cores have been drilled, the resulting holes shall be filled with econocrete or non-shrink grout material, as approved by the Engineer.

306-6.1.4  Grade Testing.  The elevations of the finished econocrete shall be surveyed on both sides of the econocrete lane, every 25 ft (7.6 m).

306-6.1.5  Surface Tolerance Testing.  After the econocrete has hardened sufficiently, it shall be tested for surface tolerance with a 16-ft (4.9-m) straightedge provided by the Contractor.

306-6.2  ACCEPTANCE CRITERIA.  Acceptance of econocrete will be based on compressive strength, thickness, grade, and surface tolerance, as described in the paragraphs below.

306-6.2.1  Compressive Strength Requirements.  The econocrete shall meet all of the following compressive strength requirements on a lot basis:

- The compressive strength of the lot, tested at 7 days, shall be greater than 500 psi (3,445 kPa).  When a given lot of econocrete fails to meet the minimum compressive strength requirements, the entire lot shall be replaced at the Contractor’s expense.

- Not more than 20 percent of the individual cylinders in a given lot, tested at 7 days, shall have a compressive strength greater than 800 psi (5,512 kPa).  When greater than 20 percent of the individual cylinders in a given lot have 7-day compressive strengths in excess of 800 psi (5,512 kPa), and transverse joints have not been constructed, a  bond-breaker shall be used.

306-6.2.2  Thickness Requirements.  The completed thickness shall be as shown on the plans.  When the average lot thickness is not deficient by more than ½ in (12.5 mm) from the plan thickness, full payment shall be made.  If the lot average thickness is deficient by more than 1 in (25.4 mm), it shall be removed and replaced at the Contractor’s expense.  When such measurement is deficient more than ½ in (12.5 mm) and not more than 1 in (25.4 mm) from the plan thickness, one additional core shall be taken at random from each sublot within the lot.  The thickness of these additional cores shall be determined as indicated in paragraph 304-6.1.2.  A new lot average thickness shall be recomputed based on these additional cores and the original cores taken from each sublot.  When the recomputed average lot thickness is not deficient by more than ½ in (12.5 mm) from the plan thickness, full payment shall be made.  If the average lot thickness is deficient by more than ½ in (12.5 mm) from the plan thickness, the entire lot shall be removed and replaced at the Contractor's expense or shall be permitted to remain in place at an adjusted payment of 75 percent of the contract unit price.

When the measured thickness is more than that indicated on the plans, it will be considered as conforming to the requirements, provided the surface of the completed econocrete layer is within the established grade and surface tolerance requirements.

306-6.2.3  Grade Requirements.  When the completed surface is more than ½ in (12.5 mm) above the grade shown in the plans, the surface shall be trimmed at the Contractor’s expense using an approved grinding machine to an elevation that falls within a tolerance of ¼ in (6 mm).  The ground surface shall be sprayed with curing compound at double the rate specified prior to paving.

306-6.2.4  Surface Tolerance Requirements.  Surface deviations shall not exceed ⅜ in (9.5 mm) from a 16-ft (4.9-m) straightedge laid in any location parallel with or at right angles to the longitudinal axis of the centerline (includes along all edges of the paving lane).  Any high spots of more than ⅜ in (9.5 mm) in 16 ft (4.9 m) shall be marked and immediately trimmed with an approved grinding machine.  If the overlying layer is PCC pavement, the ground surface shall be sprayed with a double application of the curing compound at the specified rate prior to paving.

#### METHOD OF MEASUREMENT

306-7.1  The quantity of econocrete to be paid for will be determined by the number of [yd2 (m2)] of econocrete actually constructed and accepted by the Engineer as complying with the plans and specifications.

#### BASIS OF PAYMENT

306-8.1  The accepted quantities of econocrete will be paid for at the contract unit price per [yd2 (m2)] for econocrete base.  The price and payment shall be full compensation for furnishing and placing all materials, provided; however, for any pavement found deficient in thickness as specified in paragraph 306-6.2.2, the reduced unit price shall be paid.

Payment will be made for econocrete base course--per [yd2 (m2)].

#### TESTING REQUIREMENTS

ASTM C 31	Making and Curing Concrete Test Specimens in the Field

ASTM C 39	Compressive Strength of Cylindrical Concrete Specimens

ASTM C 136	Sieve or Screen Analysis of Fine and Course Aggregates

ASTM C 172	Sampling Freshly Mixed Concrete

ASTM C 173	Air Content of Freshly Mixed Concrete by the Volumetric Method

ASTM C 174	Measuring Length of Drilled Concrete Cores

ASTM C 192	Making and Curing Concrete Test Specimens in the Laboratory

ASTM C 231	Air Content of Freshly Mixed Concrete by the Pressure Method

ASTM D 560	Standard Test Methods for Freezing and Thawing Compacted Soil-Cement Mixtures

ASTM D 3665	Random Sampling of Paving Materials

AASHTO T 26	Quality of Water to be Used in Concrete

#### MATERIAL REQUIREMENTS

ASTM C 33	Specification for Concrete Aggregates

ASTM C 94	Specification for Ready-Mixed Concrete

ASTM C 150	Specification for Portland Cement

ASTM C 260	Specification for Air-Entraining Admixtures for Concrete

ASTM C 309	Specification for Liquid Membrane-Forming Compounds for Curing Concrete

ASTM C 494	Specification for Chemical Admixtures for Concrete

ASTM C 595	Standard Specification for Blended Hydraulic Cements

ASTM C 618	Specification for Fly Ash and Raw and Calcined Natural Pozzolans for Use in Portland Cement Concrete

ASTM C 989	Standard Specification for Ground Granulated Blast-Furnace Slag for Use in Concrete and Mortars

### END P-306