DRAFT									ATTACHMENT B

# Technical Specifications for Thermal Infrared Sensor (TIRS) Lenses

## Background

Preliminary lens requirements for the TIRS instrument on board the Landsat Data Continuity Mission (LDCM) are given below. Lens specifications are chosen in order to produce a diffraction-limited focus for an ideal, on-axis input beam in a 25 μm square pixel. The operational, or in-band, wavelength of the telescope is 10.3 – 12.5 μm.

The contractor will provide:

- Four (4) Ge lenses according to the L1 design

- Four (4) ZnSe lenses according to the L2 design

- Two (2) Ge lenses according to the L3 design

- Two (2) Ge lenses according to the L4 design

## Environment

The lenses will be used at an operational temperature of 160 ± 1 K. Lenses must be capable of temperature cycling between room temperature and 77 K at least 25 times without changing their performance.

## Surface figure and coatings

All four lenses are to be ground and polished to the figure given in each technical drawing below. Anti-reflection coatings will provide <1.5% reflection from any surface for the in-band wavelengths and >94% average transmission for each lens for the in-band wavelengths for an on-axis in-band source.

The relative in-band transmission shall not change by more than ± 10% of its original value over 3 years and a total radiation dosage of 25 krad.

## Metrology and delivery

The contractor is required to perform all necessary measurements to verify that lenses meet all specifications. A report including the required quality assurance data and documenting the various measurements and their analysis will be included with each delivery, including separate serial numbers and a certification log for each lens. Lenses shall be delivered to Goddard Space Flight Center (GSFC) in shipping / storage containers that are suitable for long-term storage of critical optical components.

12/17/08