U.S. General Services Administration
Federal Supply Service
Paints and Chemicals Center
400 15th St. SW
Auburn, WA  98001-6599
1-800- 241-RAIN (7246)

COMPARISON OF MULTI PURPOSE ADHESIVES, COST,  
ENVIRONMENTAL ATTRIBUTES AND PERFORMANCE CHARACTERISTICS

GSA handles many types of general purpose adhesives. The three tables below summarize information on the one component (non-epoxy) category of these products.  These glues are recommended for light stress, non structural uses.

TABLE I.  PRICE COMPARISON

| BRAND or SPEC | NSN 8040- | SIZE | mL | PRICE | cents/mL |
| --- | --- | --- | --- | --- | --- |
| A-A-1270 | 00-781-8889 | 4 OZ | 118 | 0.42 | 0.03 |
| A-A-1270 | 00-754-2485 | QT | 946 | 2.45 | 0.26 |
| A-A-1270 | 00-754-2483 | 8 OZ | 236 | 0.84 | 0.35 |
| A-A-1270 | 00-774-8557 | GL | 3780 | 15.17 | 0.40 |
| MMM-A-1617A Ty III | 00-281-1977 | 5 GL | 18900 | 92.36 | 0.49 |
| MMM-A-121 | 00-843-3461 | GL | 3780 | 19.18 | 0.51 |
| MMM-A-1617A Ty III | 00-273-8697 | GL | 3780 | 22.12 | 0.58 |
| A-A-1270 | 00-754-2484 | 8 OZ | 236 | 1.40 | 0.59 |
| MMM-A-121 | 00-165-8614 | QT | 946 | 5.97 | 0.63 |
| A-A-863 | 00-266-7429 | PT | 473 | 3.33 | 0.69 |
| MMM-A-1617A Ty I | 00-281-1972 | GL | 3780 | 26.55 | 0.70 |
| HERCULITE CVV | 00-159-4884 | QT | 946 | 7.13 | 0.75 |
| MMM-A-121 | 00-273-8717 | PT | 473 | 3.55 | 0.75 |
| MMM-A-1617A Ty II | 00-290-4301 | QT | 946 | 7.21 | 0.76 |
| MMM-A-1617A Ty III | 00-262-9011 | PT | 473 | 3.90 | 0.82 |
| MMM-A-121 | 00-273-8716 | .5 PT | 236 | 2.27 | 0.96 |
| ASHLAND PLIOBOND 20 | 00-200-4574 | GL | 3780 | 36.54 | 0.97 |
| DEXTER 1942 SUPERSTIK | 01-214-4075 | 12 stks | 472 g | 5.18 | 1.10 |
| MMM-A-1617A Ty III | 00-298-1946 | 8 oz | 236 | 2.62 | 1.11 |
| MMM-A-1617A Ty I | 00-262-9028 | PT | 473 | 6.02 | 1.27 |
| 3M 847 | 00-691-6134 | GL | 3780 | 54.88 | 1.45 |
| 3M 847 | 00-390-7959 | QT | 946 | 14.18 | 1.50 |
| ASHLAND PLIOBOND 20 | 00-200-9190 | QT | 946 | 15.1 | 1.60 |
| MMM-A-189 | 00-043-1717 | 2 oz | 59 | 5.72 | 1.69 |
| 3M EC 1300 | 01-023-4173 | PT | 473 | 8.58 | 1.81 |
| ASHLAND PLIOBOND 20 | 00-680-1080 | 3.75 oz | 110 | 2.51 | 2.28 |
| 3M 847 | 01-416-1092 | BX | 5310 | 134.2 | 2.52 |
| GLYPTAL 1276 | 01-199-1642 | GL | 3780 | 98.28 | 2.60 |
| 3M 847 | 01-033-7507 | 5 oz | 147.5 | 3.93 | 2.66 |
| MMM-A-182 | 00-266-0856 | 8 oz | 236 | 6.54 | 2.77 |
| MMM-A-121 | 00-832-6173 | 5 oz | 147.5 | 4.15 | 2.8 |
| MMM-A-1617A Ty I | 00-262-9025 | 4 OZ | 118 | 3.99 | 3.38 |
| MMM-A-1617A Ty II | 00-221-3811 | 2 oz | 59 | 2.45 | 4.15 |
| BOSTIK 4024 | 00-942-9137 | 16 oz | 473 | 20.97 | 4.43 |
| HERCULITE CVV | 00-159-4885 | 1.5 oz | 44 | 3.08 | 6.96 |

TABLE II. PRODUCT USES AND FEATURES:

| BRAND or SPEC | TYPE | USE |
| --- | --- | --- |
| 3M 847 | RUBBER | Multipurpose acrylonitrile adhesive, bonds leather, nitrile rubber, plastics, gaskets mylar. Forms strong, flexible bonds, resists fuels and oil, can heat cure 2 min@400F |
| 3M EC 1300 | RUBBER | Spray or brush application, synthetic elastomer base, heat resistant, bonds neoprene, reclaimed/butyl rubber, wood, metal, plastic. Salt water resist.Epoxy graphite skin repair, night vision sights. |
| A-A-1270 | POLYVINYL | General purpose white glue |
| A-A-863 | RUBBER | Bonding paper, large charts |
| ASHLAND PLIOBOND 20 | RUBBER | Bonds metal, glass, rubber, ceramics, paper, leather, concrete, fabric. Thermoplastic/synthetic rubber based, 400% elongation, resists chemicals, fuels, turpentine, oils. Heat cure at 175F for stronger bonds |
| BOSTIK 4024 | RUBBER | Fast drying, bonds fibrous, porous, nonporous like metal, wood, fabric, laminate films, foils, foams, fabrics, rigid sheet stock, velcro tape to wood. Water/oil resist |
| DEXTER 1942 SUPERSTIK | HOT MELT | Hot melt sticks. Ethylene vinyl acetate based adhesive, bonds wood, plastics (nylon, polycarbonate, PVC, polystryene, ABS, acrylic. 500% elongation. |
| GLYPTAL 1276 | NITROCELLULOSE | Bonds porcelain, leather, paper, cloth, metals, plastics. Not for rubber. Electrically insulating. Water and oil resistant. |
| HERCULITE CVV | RUBBER | Nitrile rubber based, bonds plastic, cloth, paper, wood, metals. Waterproof |
| MMM-A-121 | RUBBER | Neoprene rubber adhesive. Bonds rubber to steel. Salt water resistant. Can heat cure 30 min@154C. |
| MMM-A-1617A Ty I | RUBBER | Natural rubber based. Bonds fabric, leather, felt, cork, steel, Al, wood, rubber, plastics, wool, natural rubber. Oil resistant. Superior bond to polychloroprene. Water/oil resistant, not fuel resistant. Strip adhesion 15 lbs/min. Dead load 2 lbs. |
| MMM-A-1617A Ty II | RUBBER | Polychloroprene rubber based, bonds fabric, leather, felt, cork, steel, Al, wood, rubber, plastics, alloy, laminates, wool, natural rubber. Oil and water resistant, not fuel resistant. |
| MMM-A-1617A Ty III | RUBBER | Butadiene acrylonitrile rubber based. Bonds fabric, leather, felt, cork, steel, Al, wood, buna-N, plastics, alloy, laminates, wool, and vinyl plastics. Resists oil, water, aromatic fuels. |
| MMM-A-182 | RUBBER | Cold bonding rubber, inner tubes. 6% nonvolatiles. |
| MMM-A-189 | RUBBER | Thermoplastic synthetic rubber adhesive for general purpose use,.20% nonvolatiles. Cure 18 hrs@rt+24 hrs@122F |

TABLE III. PERFORMANCE CHARACTERISTICS AND ENVIRONMENTAL ATTRIBUTES

| BRAND or SPEC | VOC | EPA 17 | OTHER | SHIP | HARD | TENSILE | TENSILE | T- | CMPRESS |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | g/L |
| HAZMAT | HAZ | NESS | STRNGTH | SHEAR | PEEL | STRNGTH |
|  | shore | psi | psi | ppi | psi |
| 3M 847 | 583 |
| A | FL |
|  | 200 | 40 |
|  | 3M EC 1300 | 550 | T,M | H | FL |
|  | 549 | 30 |
|  | A-A-1270 | 0 |
| 2750 |
| 17200 |
| A-A-863 | 700 |
| HP, I | FL |
|  | ASHLAND PLIOBOND 20 | 700 | M |
| FL | 82 A | 1500 | 500 | 33 |
|  | BOSTIK 4024 | NA | M | A,B | FL |
|  | DEXTER 1942 SUPERSTIK | 0 |
|  | 250 |
|  | GLYPTAL 1276 | 597 | T,M | EA,I,DBP,E | FL |
|  | HERCULITE CVV | 644 | T | A | FL |
|  | MMM-A-121 | 630 | T | H,E,A | FL |
| 4 |
|  | MMM-A-1617A Ty I | 465 | T,M | H | FL |
| 12 |
|  | MMM-A-1617A Ty II | 571 | T,M | H,A | FL |
|  | MMM-A-1617A Ty III | 677 | T,M | EA | FL |
|  | MMM-A-182 | 611 | T,M | H,A | FL |
| 25 |
|  | MMM-A-189 | 700 | T,M |
| FL |
|  | 1200 | 12 |

Chemicals:

T - toluene, M - methyl ethyl ketone, A - acetone, B - butanol, H - hexane, HP - heptane E - ethanol, EA - ethyl acetate, DBP - dibutlyl phthalate, I - isopropyl alcohol

FL = flammable liquid

Values given are per manufacturer’s data sheet or specification requirements, room temperature cure and service temperature.