U.S. General Services Administration
Federal Supply Service
Paints and Chemicals Center
400 15th St. SW
Auburn, WA  98001-6599
1-800- 241-RAIN (7246)

COMPARISON OF MULTI PURPOSE EPOXY TWO PART ADHESIVE KITS, COST, ENVIRONMENTAL ATTRIBUTES AND PERFORMANCE CHARACTERISTICS.

TABLE I. PRICE COMPARISON

| BRAND/SPEC | NSN 8040- | SIZE | COST | mLs | CENTS/ML |
| --- | --- | --- | --- | --- | --- |
| ASTM C881 TYI | 00-138-7982 | 0.5 GL | 8.06 | 1890 | 0.43 |
| EPIPHEN 825-A/7517 | 01-406-8119 | QT | 5.14 | 946 | 0.54 |
| MMM-A-134 Ty II | 00-998-3339 | GL | 56.57 | 3780 | 1.50 |
| MMM-A-134 Ty III | 00-881-0804 | GL | 81.75 | 3780 | 1.62 |
| MMM-A-134 Ty I | 00-270-8137 | QT | 15.29 | 946 | 1.62 |
| MMM-A-134 Ty III | 01-027-4901 | QT | 17.07 | 946 | 1.80 |
| DEXTER EPK 0151 | 00-145-0043 | 2 QT | 37.69 | 1892 | 1.91 |
| HB FULLER 7004 | 00-062-4173 | QT | 23.16 | 946 | 2.45 |
| DEXTER EPK 608 | 00-539-7798 | 6 oz | 4.80 | 177 | 2.71 |
| DEXTER EPK 11C | 01-004-1031 | 4 oz | 3.47 | 118 | 2.94 |
| MMM-A-134 Ty II | 01-036-3771 | 4 oz | 3.57 | 118 | 3.02 |
| DEXTER EPK 0151 | 01-066-6442 | GL | 120.59 | 3780 | 3.19 |
| DEXTER EPK 1C | 00-777-0631 | 4 oz | 4.03 | 118 | 3.41 |
| MMM-A-134 Ty III | 00-142-9207 | 8 oz | 8.76 | 236 | 3.71 |
| C-7/W | 00-564-5374 | 2 QT | 69.76 | 1892 | 3.69 |
| K-20 | 01-057-0092 | 5 oz | 6.97 | 147.5 | 4.72 |
| A-A-3053 TYI | 00-753-4800 | 1.5 oz | 2.10 | 44.25 | 4.74 |
| DEXTER EPK 0151 | 00-061-8303 | 3.35 oz | 5.57 | 98 | 5.68 |
| A-A-3053 TY II | 00-846-3351 | PT | 30.08 | 473 | 6.36 |
| MMM-A-134 Ty II | 00-270-8136 | QT | 65.68 | 946 | 6.94 |
| MT-13 | 00-028-8630 | 5 oz | 11.25 | 147.5 | 7.63 |
| A-1/A | 00-809-0701 | QT | 79.75 | 946 | 8.43 |
| A-A-3053 TY II | 01-048-3158 | 5 oz | 12.5 | 147.5 | 8.47 |
| C-7/W | 00-180-6200 | QT | 80.87 | 946 | 8.55 |
| MMM-A-134 Ty II | 00-691-1322 | PT | 41.63 | 473 | 8.80 |
| SUPER INSTANT EPOXY | 01-134-0434 | 5 oz | 14.25 | 147.5 | 9.66 |
| MMM-A-134 Ty I | 00-157-8677 | 2.5 oz cart | 9.16 | 74 | 12.38 |
| 3M DP 110 | 01-332-0774 | 1.95 oz | 8.34 | 57.5 | 14.50 |
| GE THORSEN 10-347 | 00-281-2308 | 4 oz | 17.58 | 118 | 14.90 |
| ECCOBOND 286 | 01-056-5320 | 3 oz | 13.34 | 88 | 15.15 |
| MMM-A-134 Ty II | 00-081-2166 | 8 oz | 38.85 | 236 | 16.46 |
| DEXTER EA 907 | 00-967-7346 | PT | 92.65 | 473 | 19.59 |
| MMM-A-134 Ty II | 00-138-8485 | 60 g | 11.53 | 60g | 19.22/g |
| K-230 | 00-061-8303 | 95 g | 5.57 | 95 g | 5.86 |
| DEXTER EPK 608 | 00-092-2816 | 100 3.5 g pkgs | 19.04 | 350 g | 5.44/g |
| TRA-CON BB 2101 | 00-883-7108 | 7 g | 5.19 | 7 g | 74.14/g |

TABLE II. PRODUCT USES AND FEATURES

| EPOXY | USE | RESISTANCE |
| --- | --- | --- |
| 3M DP 110 | Machinable, clear liquid, for bonding clear subtrates, potting and encapsulating where flexibility is required, use in EPX applicator |
|  | A-1/A | Liquid, bonds metals, wood, glass, ceramics, hard rubber, thermoset plastics, good for hard to bond, rigid substrates | W,C,S |
| A-A-3053 Ty I | low strength, non structural bonds to metals, porcelain, ceramics, leather, wood, porous/nonporous, nonsag. |
|  | A-A-3053 Ty II | intermediate strength, nonstructural bonds to metals, porcelain, ceramics, leather, wood, porous/nonporous, non sag |
|  | C-7/W | Transparent liquid bonds wood, plastic, rubber, metal, cement, cryogenic applications. Keep frozen. |
|  | DEXTER EA 907 | Paste, bonds rubber, plastic, wood, glass, metal, poorly prepared surfaces |
|  | DEXTER EPK 0151 | Optically clear liquid, bonds glass, metal, plastic, phenolics. Repair/coat circuit boards. Bonds materials w dissimilar expansion. | C,O,S |
| DEXTER EPK 11C | black paste used to fill key slot on machine gun mount |
|  | DEXTER EPK 1C | Paste, bonds metals, woods, rubber, plastic. Can sand, cut, tape, machine | W |
| DEXTER EPK 608 | Reading clear liquid, fast setting, high strength, use on Pratt & Whitney turbofan engines, required on ships for metal to fiberglass bonding |
|  | ECCOBOND 286 | white paste, bonds metal or plastic pipes to replace solder, solvent adhesives or brazing. |
|  | EPIPHEN 825-A/7517 | tan liquid, bonds metals, glass, ceramics, plastics. High tensile shear strengths. kit consists of resin, modifier, filler, curing agent | Sa |
| EPOXYLITE 203/301 | black paste, 0.1% water absorption, used to bond broken ceramic bushings, seal cracks in diesel engine a-frames, seal leaking transformers, repair glass lined vats |
|  | GE THORSEN 10-347 | gray silica filled sag resistant paste, fill cracks, good electrical, thermal, chemical resistance, high mechanical strength in wet conditions | W,C,O |
| HB FULLER 7004 | Liquid, bonds rigid/flexible surfaces, metals, leather, rigid plastic, concrete, glass, ceramics, wood, rubber , wood lamination for sporting goods, potting small electronic parts. Cleavage strength 1050psi. | W,C |
| K-20 | clear epoxy adhesive for bonding aluminum.0.4% water absorption, 0.7% linear shrinkage | W,C,O,S |
| K-230 | optically clear, bonds glass, metal, plastic and phenolics, elastomerics to rigid substrates |
|  | MMM-A-134 | Structural adhesive for bonding aluminum alloys on aircraft for high strength joints. Also bonds wood, glass and resin laminates Ty I, RT cure, Ty II/III, 210F cure | Sa, W, C, O, So |
| MT-13 | White sag resistant paste for porous and nonporous surfaces, water resistant bonds. Elasticity (Tension)285000, Elasticity (Compression) 165000 | W |
| SUPER INSTANT EPOXY | Amber liquid, fast (mercaptan) cure, rapid bonding of steel, aluminum, brass, wood, masonry, hard plastics. Not for nickel, Cr, tin, zinc or soft thermoplastics. 10% elongation.27M modulus of elasticity (tension), 115M modulus of elasticity (compression) |
|  | TRA-CON BB 2101 | Tan liquid, bonds metal, glass, ceramic, wood, marble, concrete, plastic. Good electrical insulator. Kit consists of resin, modifier, filler, curing agent | Sa, W, C, O, So, F |

RT - room temperature Sa - Salt spray, W - water/humidity, F - fuel, C - chemicals (acid, base, bleach, etc.), O - oils, lubricants, So - solvents

TABLE III. PERFORMANCE CHARACTERISTICS

| SPEC | HRD | TEN | TEN | T- | DRM | FLX | CMP | MAX | DLCT | DLCT | TRM |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | NES | STR | SHR | PEL | PEL | STR | STR | TMP | CNS | STR | CND |
| 3M DP 110 |
|  | 2500 | 20 |
| 520 |
|  | A-1/A |
| 3000 | 1600 |
| 15200 |
| A-A-3053 Ty I |
|  | 100 |
| A-A-3053 Ty II |
|  | 400 |
| C-7/W |
| 4420 | 4310 |
| 18500 |
| DEXTER EA 907 |
|  | 3300 |
|  | 180F |
|  | DEXTER EPK 0151 |
|  | 1950 |
|  | 11000 | 19000 |
| 3.35 |
| DEXTER EPK 11C | 80D |
| 1750 |
| 6.11 |
| DEXTER EPK 1C |
|  | 1750 |
|  | 300F | 6.11 |
| DEXTER EPK 608 |
|  | 2000 | 12.3 |
| 125F | 4.1 |
| ECCOBOND 286 |
|  | 2200 |
|  | 12000 |
| 220F |
|  | EPIPHEN 825-A/7517 |
|  | 3000 |
| EPOXYLITE 203/301 | 35 Bar | 8000 | 2500 |
|  | 18000 | 16000 |
| GE THORSEN 10-347 |
| 390F |
| 300 |
|  | HB FULLER 7004 | 85D | 4575 |
| 1.5 | 13 | 9400 | 19300 |
| K-20 | 75 D |
| 1950 |
|  | 6000 | 10000 |
| 5.7 |
| K-230 |
| 2000 |
| 10000 | 18000 |
| 3.35 | 2000 |
|  | MMM-A-134 Ty I |
|  | 2500 |
| MMM-A-134 Ty II |
|  | 2500 |
| MMM-A-134 Ty III |
|  | 2500 |
| MT-13 | 72 Bar | 4300 | 3100 |
| 8700 |
| SUPER INSTANT EPOXY | 60 Bar | 1100 | 2900 | 4500 |
|  | 4500 |
| TRACON B-B 2101 | 85 D |
| 4.3 | 370 |

Tests at room temp. Units as listed below.  Information  for brand name items from manufacturer data sheets.

Hardness, Shore D or Barcol; Tensile Strength, psi,Al; Tensile Shear psi, Al/Al; T-Peel, pli; Climbing Drum Peel, pli; Flexural Strength, psi; Compressive Strength, psi; Maximum Service Temperaure, (F, ; Dielectric Constant, 1 khz; Dielectric Strength, volts/mil; Thermal Conductivity, Cal cm/cm2 sec (C 10 -4.

TABLE IV. ENVIRONMENTAL CHARACTERISTICS

All epoxy products contain bisphenol A epichlorohydrin epoxy resin and have a low VOC, usually less than 10 grams per liter.

| EPOXY | HAZARDOUS CHEMICALS | SHP HZ |
| --- | --- | --- |
| 3M DP 110 | 2,4,6-tri(dimethylaminomethyl)phenol, terphenyl plasticizer | corrosive |
| A-1/A | diethylenetriamine | none |
| A-A-3053 Ty I | tertiary amine phenol derivative | none |
| A-A-3053 Ty II | polyamide resin | none |
| C-7/W | amide | frozen |
| DEXTER EA 907 | silica, titanium dioxide, triethylenetetramine | none |
| DEXTER EPK 0151 | butyldiglycidyl ether, silicon dioxide, polyamide resin, triethylenetetramine, tetraethylenepentamine | corrosive |
| DEXTER EPK 11C | silica, diethylenetriamine | corrosive |
| DEXTER EPK 1C | diethylenetriamine | corrosive |
| DEXTER EPK 608 | ethylene glycol, 2,4,6 tri(dimethylaminoethyl)phenol | none |
| ECCOBOND 286 | diethylene glycol di (3-aminopropyl) ether | corrosive |
| EPIPHEN 825-A/7517 | dialkylamine and dialkylene triamine | none |
| EPOXYLITE 203/301 | Mg silicate, silicon dioxide, diethylenetriamine | corrosive |
| GE THORSEN 10-347 | triethylenetetramine, silica dioxide | none |
| HB FULLER 7004 | triethylenetetramine | corrosive |
| K-20 | diethylene triamine | corrosive |
| K-230 | triethylenetetramine, butyl glycidyl ether, silica | none |
| MMM-A-134 Ty I | calcium carbonate, amorphous silica, polyamide | none |
| MMM-A-134 Ty II | diethyleneaminopropylamine, m-dihydroxybenzene, phenyl glycidyl ether | none |
| MMM-A-134 Ty III | calcium carbonate | none |
| MT-13 | silicon dioxide, talc, tremolite | none |
| SUPER INSTANT EPOXY | 1,4 diazabicyclo (2,2,2,)octane | none |
| TRA-CON BB 2101 | diethylenetriamine | none |

Italics: named as a carcinogen on MSDS