Preservation Note 25

Repair of Scratched Limestone

Masonry

June-98

Masonry Restoration and Cleaning-04900

Scratched Limestone

--------------------------------------------------------------------------------

In the summer of 1992, damage to a section of exterior limestone wall occurred along a ramp to a loading dock at the Department of Interior building. The damage resulted in deep (up to 1/2") scratches in the limestone but fortunately; careful inspection by qualified persons uncovered no cracking of the stones or mortar joints. In consultation with the GSA Regional Historic Preservation Staff, the Department of Interior honed the damaged area to eliminate the scratches. When completed, the honed surface matched the adjacent aged limestone. However in fall 1993, follow-up inspections by DOI and GSA Regional Historic Preservation Staff revealed a marked difference in appearance of the honed limestone. A year of weathering had highlighted differences in texture between the honed surface and the aged limestone. The honed surface texture had, over the year, become more reflective or smoother as it weathered. This high contrast effect highlighted the precise area where repair had been attempted.

--------------------------------------------------------------------------------

Currently, the repair attempt is significantly more noticeable than the original damage. Future weathering will continue to modify the appearance of the limestone.

CONCLUSIONS

1. Because abrasive scratch repair methods such as honing, waterblasting, or sandblasting change the surface texture of the stone, areas repaired with these methods may become more noticeable over time than the original scratch. Experiences at the Department of Interior Building indicate that the guiding principle for repairing scratches in exterior limestone may be to simply clean the stone non-abrasively to diminish the visibility of the scratches, and then monitor the damage.

2. Annual scheduled inspection accompanied by clear photographic documentation every year will permit buildings management / architects / facilities management to re-evaluate the condition of the damaged area. This inspection and documentation over several years will indicate if the damaged area is becoming less noticeable or more noticeable, via accelerated deterioration or intensified staining.

3. Extent of damage, depth and direction of scratches (horizontal, diagonal, vertical); exposure to the sun, rain, wind; building detailing; and time will all help to determine the visual effect of the damage. A single scratch may be less noticeable than a repair.

4. The decision to monitor damage may affect the Government's ability to file claims for damages with the Contractor. Depending on the potential cost of the claim, the Contracting Officer may want to consider amending the contract to include the monitoring period. Thorough documentation of the damage will assist the Contracting Officer in making this determination. When only scratches are involved, monitoring the damaged area is the preferred choice of action.