Preservation Note 36

Wood Refinishing

Wood & Plastics

June 99

Wood Restoration and Cleaning - 06900

Part 1: General

1-1 Description: Work in this section includes:

Strip and refinish sills, paneling, casework, moldings, and handrails in the Main Interior Building Library Reading Room.

All work is to be performed between 5:30 p.m. and 2:30 a.m. or on the weekends.

Because the library will be operational throughout the restoration process, minimize area affected by the refinishing.

Provide scaffolding as required.

1-2 Submittals

Material Safety Data Sheets.

Product Specification Data Sheets for review and approval.

Provide a proposal for review and approval that addresses refinishing methods and schedule. (See Competency of Bidder form AA par. 3)

Finished 4' X 4' sample panel in place to the satisfaction of the COTR.

1-3 Measurements:

Take all required field measurements and verify profiles and installation conditions for work of this section.

1-4 Job Conditions:

Determine that surfaces to which finishes are to be applied are even, smooth, sound, clean, dry, and free from defects affecting proper application. Correct or report defective surfaces to Contracting Officer's Technical Representative.

1-5 Trash Removal:

Remove all debris from the site daily.

1-6 Safety:

Contractor is responsible for safety program.

1-7 Codes:

Comply with all Federal and local regulations.

Part 2: Materials

2-1 Stain:

Oil penetrating stain, such as "Mini-Wax"; if required - test panel will determine use.

2-2 Solvent:

Chemical stripper such as "Peel Away-Five" or "E-Z" paint and varnish remover.

2-3 Finish:

TR-1 Finish ( American Wood Institute Finish System) to match original matte sheen. Sample panel will determine use of spray applicator.

2-4 Bronze Wool:

Grade 000.

2-5 Cloth

Clean cotton waste.

Treated track cloth to remove sanding dust prior to finishing.

Store all flammable materials off-site.

Part 3: Execution

3-1 Stripping Varnish (From Damaged Library Paneling, Molding, Casework, and Handrails)

Preparation:

Make sure work area is well ventilated and wear protective clothing and rubber gloves. Smoking is not allowed in the work area. Place fire extinguisher for Class B fires at work locations for emergency use.

Work area should be within a comfortable arm reach. Protect areas of wood adjacent surfaced not to be refinished from solvent and other stripping operations.

Fill scratches and gouges with shellac burn-in sticks matching the color to the wood stain.

Wood Refinishing:

Per contractor's approval proposal.

Fill scratches and gouges with shellac burn-in sticks matching the color to the wood stain

Marty Shore and Brian Blundell