## Section 313. — Aggregate-Topsoil Course

08/01/14– FP-14

WFL Specification 07/17/14

Include the following when seed is not required in the mixture.

Description

### 313.01

Delete the text of this Subsection and substitute the following:

This work consists of furnishing and placing an aggregate and topsoil mixture on a prepared shoulder or other surface.

Material

### 313.02

Delete the text of this Subsection and substitute the following:

Conform to the following Subsection:

Crushed aggregate 703.06

Topsoil 713.01

Water 725.01(c)

Construction Requirements

### 313.04 Mixing, Placing, and Compacting.

Delete the text of this Subsection and substitute the following:

Furnish a mixture of 50±10 percent aggregate and 50±10 percent topsoil by volume with sufficient water for compaction.

Mix the components into a uniform mixture. Spread the mixture on the prepared surface in a uniform layer. Shape the mixture to the line, grade, and cross-section. Remove clods and stones greater than 2 inches (50 millimeters) in diameter.

Uniformly compact the mixture to ensure that it does not exhibit heaving, pumping, rutting, or shearing. Compaction tests may be waived by the CO if acceptable compaction is demonstrated.

Remove all material from the pavement surface upon completion.

WFL Specification 06/02/14

Include the following when aggregate-topsoil is required.

### 313.05 Acceptance.

Delete the text of this Subsection and substitute the following:

Crushed aggregate will be evaluated under Subsections 106.02 and 106.03

Topsoil will be evaluated under Subsections 106.02 and 106.03.

Construction of aggregate-topsoil course will be evaluated under Subsection 106.02.