## Section 712. — Joint Material

11/05/15–FP14

WFL Specification 11/05/15

Include the following on AK DOT&PF Projects when Section 564 work is required.

### 712.01.

Add the following:

**(h) Expanded polyethylene.** Use closed-cell expanded polyethylene with a density of at least 2.1 lb/ft3 as determined by ASTM D3575 and with a minimum compressive stress of 9 psi at 25% deflection as determined by ASTM D3575.