# DIVISION 500 RIGID PAVEMENTS

## Section 501. — RIGID PAVEMENT

Description

501.01  This work consists of constructing rigid pavement on a prepared surface.  This work also includes pavement rehabilitation consisting of full-depth, full-width removal and reconstruction of rigid pavement.  Pavement smoothness/roughness type is designated as shown in Subsection 501.12.

Material

501.02 Conform to the following Subsections:

Air-entraining admixtures	711.02

Chemical admixtures	711.03

Coarse aggregate	703.02

Curing material	711.01

Epoxy grout	725.22(b)

Epoxy resin adhesives	725.21

Fine aggregate	703.01

Fly ash	725.04(a)

Hydraulic cement	701.01

Joint fillers and sealants	712.01

Non-shrink grout	725.22(c)

Reinforcing steel, tie bars, dowel bars, hook bolts, caps	709.01

Water	725.01

Construction Requirements

501.03  Composition of Mix (Concrete Mix Design).  Design the concrete mix according to Subsection 552.03.  Conform to Table 501-1.

501.04  Equipment.  Furnish equipment conforming to the following:

(a) Forms.  Furnish straight, steel forms.  For edge radii less than 60 meters, furnish flexible or curved forms.  Conform to all the following:

(1) Depth equal to edge of pavement thickness;

(2) 3-meter minimum length;

(3) Stabilizing devices to withstand paving operations;

(4) Joint locks to join form lengths tightly together; and

(5) Clean and oil before each use.

Table 501-1

Rigid Pavement Composition

| Water/Cement Ratio (maximum) | Temperature of Concrete | Slump | Air Content (%) | Aggregate Size(1) (AASHTO M 43) | 28-Day Compressive Strength (minimum) |
| --- | --- | --- | --- | --- | --- |
| 0.49 | 20±10 ºC | 40±20 mm | 4½ min. | No. 57 or 67 | 25 MPa |

(1) Other AASHTO M 43 aggregate sizes smaller than no. 57 or 67 may be used in the concrete mix design.  If the nominal-maximum-sized aggregate is 12.5 millimeters or smaller, provide at least 5 percent air content.

(b) Paving.  Furnish the paving and finishing equipment applicable to the type of construction as follows:

(1) Slip form construction.  Furnish slip form machines capable of spreading, consolidating, screeding, and float-finishing the freshly-placed concrete in one complete pass of the machine to provide a dense and homogeneous pavement with minimal hand finishing.

Equip the paving machine with the following:

(a) Electronic controls to control line and grade from either or both sides of the machine.

(b) Vibrators to vibrate the concrete for the full width and depth of the strip of pavement being placed.

(c) A positive interlock system to stop all vibration and tamping elements when the forward motion of the machine is interrupted.

Operate the paving machine with a continuous forward movement and coordinate mixing, delivering, and spreading concrete to provide uniform progress without stopping and starting the paving machine.  Apply no tractive force to the machine except that which is controlled from the machine.

(2) Side form construction.  Furnish mechanical, self-propelled spreading and finishing machines capable of compacting and finishing the concrete with minimal hand finishing.  Equip the machine with one 450-millimeter minimum width screed with compensating springs to minimize the effect of the screed's momentum on the side forms, or 2 independently-operated screeds.

Coordinate the number of driving wheels, power of the motor, and the machine's mass to prevent slippage.  Any machine that displaces the side forms will not be permitted.

(3) Vibrators.  Furnish internal immersed tube or multiple spud type vibrators for all paving more than 200-millimeters-thick.  Surface pan type vibrators are acceptable for full-width concrete consolidation of slabs 200 millimeters or less in thickness.  Attach vibrators to the spreader or finishing machine or mount on a separate carriage.  For construction of irregular areas, use hand-held vibrators according to Subsection 552.11(d).

(c) Joint sealing.  Furnish sealing equipment according to the sealant manufacturer's recommendations.

(d) Joints and concrete removal.  Furnish an adequate supply of concrete saws with sufficient power to saw full depth and complete the work with water-cooled, diamond-edged blades or abrasive wheels.  Equip saws with blade guards and guides or devices to control alignment and depth.  Furnish and maintain standby equipment and an adequate supply of replacement blades or wheels.

(e) Concrete removal.  Furnish concrete saws, drop hammers, hydrohammers, and jack hammers to break concrete.  Concrete saws shall conform to (d) above.  Ball-drop breakers are not permitted.

Furnish equipment that will not damage the subgrade, subbase, base, or existing concrete slabs designated to remain.

If new or existing slabs not scheduled for replacement are chipped, spalled, or damaged during the removal operations, replace the damaged slabs.

501.05  Preparing Roadbed.  Prepare the roadbed according to Subsection 303.07 and Section 301.  Uniformly dampen the roadbed before placing the concrete.  If traffic is allowed to use the prepared roadbed, check and correct the surface immediately before the concrete is placed.

Full-depth, full-width reconstruction shall conform to Subsection 501.13.

501.06  Placing Concrete.  For storing, handling, batching, and mixing material and delivering concrete, conform to Subsections 552.04 through 552.08 and 552.10.

Do not place concrete on frozen subgrade.  Place concrete with side form or slip form paving machines.  Where a paving machine is impractical, place concrete according to Subsection 501.07.

When concrete is placed adjoining a previously-constructed lane of pavement, do not allow mechanical equipment to be operated on the existing lane until the lane has attained a minimum flexural strength of 3.8 megapascals according to AASHTO T 97 or compressive strength of 24 megapascals according to AASHTO T 22.  Protect the previously constructed lane from damage by the paving equipment.

Construct reinforcing steel according to Section 554.  Firmly position the reinforcement on acceptable supports before placing the concrete, or after spreading, mechanically place or vibrate the reinforcement to the required depth in the plastic concrete.

501.07  Construction of Irregular Areas.  In irregular areas or areas inaccessible to paving equipment, construct the pavement using side forms.  Strike-off, consolidate, float, and surface finish the concrete as follows:

(a) Thoroughly and uniformly vibrate and compact the concrete during placement without segregating the material.

(b) Using templates or screeds, strike-off the concrete to shape it to the required cross-section between the forms.  Carry a slight excess of concrete in front of the leading edge of the template or screed.

(c) Float the surface to the required grade and cross-section.

(d) Finish the surface according to Subsection 501.09.

501.08  Joints.  Do not vary longitudinal joints more than 13 millimeters and transverse joints more than 6 millimeters from the true alignment.  When curbs or medians are constructed integral with the pavement, construct transverse joints continuous through the curb or median.  Protect all joints from the intrusion of deleterious matter until sealed.

Form isolated joints at structures by placing 13-millimeter expansion joint filler around each structure that extends into or through the pavement before concrete is placed.

Remove and replace all newly-placed concrete pavement where uncontrolled cracking occurs.

(a) Longitudinal joints.  Construct longitudinal joints by forming or sawing.  Construct sawed longitudinal joints (with tie bars) when the concrete pavement placement width exceeds 4.5 meters. Construct the longitudinal joint continuous with no gaps in either the transverse or longitudinal joints at intersections.

Place tie bars perpendicular to the longitudinal joints with mechanical equipment or rigidly secured chairs without damaging or disrupting the concrete.  Do not paint or coat tie bars with any material or enclose them in tubes or sleeves.

Where adjacent lanes of pavement are constructed separately, use slip form paving machines or steel side forms to form a keyway along the construction joint.  Tie bars may be bent at right angles against the form of the first lane constructed and straightened into final position before placing concrete in the adjacent lane.  Repair or replace broken or badly-damaged tie bars.

Threaded hook bolts may be used instead of tie bars.  Fasten hook bolts to the form of the longitudinal construction joint.  With slip form paving, tie bars may be hydraulically inserted through metal keyways.

(1) Formed joints.  Form joints with an approved nonmetallic or removable device while the concrete is plastic.  When adjacent lanes are constructed separately, form the sealant reservoir in the lane placed last.

(2) Sawed joints.  After placing concrete, saw joints as soon as equipment can be supported and before uncontrolled cracking occurs.  Do not ravel the joints while sawing.  Saw longitudinal joints immediately after sawing transverse joints.  Protect the sawed concrete faces from drying during the curing period.  Saw sealant reservoirs no sooner than 72 hours after placing the concrete.

If necessary, continue sawing day and night, regardless of weather conditions.  Clean the saw cut and adjacent concrete surface of slurry residue after sawing each joint.

Do not saw a joint if a crack occurs at or near the joint location before sawing.  Discontinue sawing when a crack develops ahead of the saw.

If a crack develops in reinforced concrete pavement, remove and replace at least a 3-meter long, full-width slab properly attached to adjacent slabs.

If a crack develops in plain concrete pavement, remove and replace a full slab properly attached to adjacent slabs.

(b) Transverse expansion joints.  Form transverse expansion joints according to (a)(1) above.  Place dowel bars through transverse joints.  Hold dowels parallel to the surface and center line of the slab by a metal device that remains in the pavement.

Dowel placement implanters may be used while the concrete is plastic provided they conform to the dowel tolerance specified.  Remove all concrete that leaks into the joint expansion space.

Install the preformed joint filler full-depth, perpendicular to the subgrade, and continuous across the full-pavement width.  Do not use damaged or repaired joint filler.  If joint filler is assembled in sections, construct without an offset between adjacent sections.

(c) Transverse contraction joints.  Where required by the contract, place dowel bars according to (b) above.  Dowel bar sleeves and finishing caps are not required.  Saw joints according to (a)(2) above.  For adjacent lanes placed separately, construct joints continuously across full width of pavement.

Concrete edges adjacent to the joint may be rounded or beveled to a radius or length as approved.  Resaw or grind any joint having an insufficient opening.  Where a joint is larger than required, furnish a larger size joint seal as approved.

(d) Transverse construction joints.  Unless an expansion joint occurs at the same location, construct a transverse construction joint at the end of each day's work or where concrete placement is interrupted for more than 30 minutes.  Do not construct a transverse joint within 3 meters of any parallel joint.

If sufficient concrete has not been mixed to form a slab at least 3 meters long when an interruption occurs, remove and dispose of the excess concrete back to the last preceding joint.

Use a metal or wooden bulkhead to form the joint, shaped to the pavement cross-section, and designed to permit the installation of dowel bars.

Install dowel bars in all transverse construction joints whose location does not coincide with the location of a transverse expansion or contraction joint.

501.09  Surface Finishing.  Protect the surface from rain damage.

After floating, check the surface of the fresh concrete with a 3-meter straightedge.  Remove high areas indicated by the straightedge.  Lap each successive check with the straightedge 1.5 meters over the previous check path.

Correct pavement edge slump in excess of 6 millimeters in 3 meters before the concrete has hardened.  If edge slump exceeds 25 millimeters on any 0.3 meter or greater length of hardened concrete, remove and replace the entire panel between the transverse and longitudinal joints.

Before the concrete has initially set, work the pavement edges on each side of transverse expansion joints, formed joints, transverse construction joints, and emergency construction joints to produce a 6-millimeter continuous radius and a smooth, dense mortar finish.  Do not use mortar buildup to round edges.

Finish the surface according to Subsection 552.14(c)(1).

501.10  Curing.  Immediately after finishing and when marring will not occur, cure the concrete for a minimum of 72 hours.  Do not leave the concrete exposed for more than one half hour during the curing period.  Cure using one of the following methods:

(a) Water method.  Cure according to Subsection 552.15(b).  Entirely cover the surface of the pavement and the edges of the slab with water saturated mats.  Extend mats at least twice the thickness of the pavement beyond the edges of the slab.  Place the mats in complete contact with the surface.  Use masses or other approved methods to maintain contact.

(b) Liquid membrane curing compound method.  Cure according to Subsection 552.15(c).  Protect sawed joints from intrusion of foreign material into the joint before sealing.  Repair damaged areas immediately with additional compound.

(c) Waterproof cover method.  Thoroughly wet the surface using a fog mist applicator.  Cover the entire surface with a waterproof cover.  Lap the cover at least 0.5 meter.  Extend the cover beyond the edges of the slab at least twice the thickness of the pavement.  Place the cover in complete contact with the surface.

Use masses or other approved methods to maintain contact.  Seal, sew, or cement lap joints to prevent opening or separating while curing.

When the air temperature is expected to drop below 2 ºC, furnish a sufficient supply of insulating material.  Insulate the pavement surface and sides to a depth that maintains a temperature above 4 ºC for 3 days.  Furnish and place continuously recording thermometers according to Subsection 552.10.

Remove forms when the concrete has hardened sufficiently to resist damage but not earlier than 12 hours after placing concrete.  Protect the sides of the exposed slabs immediately with a curing method equal to that provided for the surface.  Prevent erosion of the base course beneath the exposed pavement edges until shoulders are constructed.

501.11  Sealing Joints.  Saw cut and seal joints before the pavement is opened to construction or public traffic.  Do not saw sealant reservoirs within 72 hours after placing concrete.

Clean each joint of all foreign material, including membrane curing compound and concrete slurry, immediately after sawing the joint.  Blow dry joints with compressed air.  Do not apply sealing material unless the joint faces are clean and surface dry.

Use preformed joint seals, silicone sealant, or hot-poured sealant for expansion joints.  Use silicone or hot-poured sealants for longitudinal and transverse contraction joints.

(a) Silicone or hot-poured sealants.  Install backer rod with a steel wheel to the depth required.  Do not stretch or twist the backer rod during installation.  Limit the length of backer rod installed to that which can be sealed during the same workday.

Place poured joint sealing material when the air temperature is over 4 ºC.  Immediately remove any excess or spilled material, and clean the pavement surface.  Do not use sand or similar material to cover the seal.

(b) Preformed joint seals.  Furnish the seal in one piece in the size specified for the joint opening.  Install seals with a lubricant adhesive covering both sides of the concrete joint.  Compress the seal to between 20 and 50 percent of its nominal width.  Install the top of the seal about 6 millimeters below the pavement surface.

Remove and replace seals that are damaged, twisted, improperly positioned, or stretched more than 3 percent.

501.12  Pavement Smoothness/Roughness.  Measure the smoothness/roughness of the final pavement surface after the concrete has sufficiently hardened and according to the designated type below.  In addition, construct all pavement surfaces to meet the requirements of (c) below.

(a) Type A smoothness (profile ride index (PRI)).  For type A pavement smoothness, furnish a California type profilograph and personnel to operate the profilograph.  The CO will direct and observe its operation.  Operate the profilograph in the “mode” such that the continuous plot produced can be reduced according to FLH T 504.  Measure in the middle portion of each lane and exclude areas according to FLH T 504.  Measure excluded areas according to (c) below.  Submit the trace to the CO.

A PRI will be calculated for each 0.1-kilometer lane of traveled way using a zero blanking-band.  The PRI will be determined according to FLH T 504.  Bumps will be located using a 10-millimeter bump template.

The upper specification limit is 380 millimeters per kilometer.  Defective areas are bumps in excess of 10 millimeters in 7.62 meters, 0.1-kilometer profile ride index greater than 450 millimeters per kilometer, or surfaces with a pay factor less than 0.75 as determined under Subsection 106.05.

(b) Type B roughness (international roughness index (IRI)).  For type B pavement roughness, furnish an inertial profiler conforming to AASHTO PP 50 and validated according to AASHTO PP51.  At least 21 days before use, submit results showing the inertial profiler conforms to AASHTO PP 51.  Furnish personnel to operate the inertial profiler according to AASHTO PP 52.  The CO will direct and observe its operation.  Measure in the middle portion of each lane.  Submit raw data files (*.ERD) that are compatible with FHWA Profile Viewer software on a compact disk to the CO.

Areas of localized roughness will be identified using a 7.62-meter moving average filter.  The difference between the 7.62-meter moving average and the reported relative elevation for every profile point will be determined.  Deviations greater than 3.81 millimeters are areas of localized roughness.

An IRI value will be determined for each 0.1-lane kilometer of traveled way.  Cattle guards and bridges not being overlayed will be excluded from the calculation of IRI and determination of localized roughness.  Measure excluded areas according to (c) below.

Defective areas are 0.1-lane kilometer segments with IRI values greater than 1.499 meters per kilometer or areas of localized roughness.

The pay adjustment factor for each 0.1-kilometer segment will be determined from Table 401-3.

(c) Type C pavement smoothness/roughness (straightedge measurement).  Use a 3-meter metal straightedge to measure at right angles and parallel to the centerline.  Defective areas are surface deviations in excess of 6 millimeters in 3 meters between any two contacts of the straightedge with the surface.

(d) Defective area correction.  Correct defective areas from paragraphs (a), (b), and (c) above.  Obtain approval for the proposed method of correction.  If no corrections are allowed, no adjustment will be made to the pay adjustment factors.

Re-measure corrected areas according to the specified type of pavement smoothness/roughness.  The smoothness/roughness value obtained will replace the original.

501.13  Full-Depth, Full-Width Patching.  Construct the pavement patch to provide a similar appearance to the existing pavement.  Prepare test panels using the same materials proposed for the work.

Begin pavement work after the test panels have been inspected and approved for appearance and the concrete mix design 28-day compressive strength is verified.

(a) Concrete removal.  For mesh-reinforced, plain dowel, or plain jointed concrete pavement, saw cut slabs full depth leaving vertical edges at the limits of the patch.

For continuously reinforced concrete pavement, saw cut the exterior transverse patch limits to a depth of 45±5 millimeters.  Do not allow the saw cut to penetrate the steel reinforcement.  Saw cut longitudinal limits full depth.  Break up the concrete with a chipping hammer down to the steel.

If replacement steel is welded, cut the existing reinforcing steel and leave 200 millimeters of steel exposed.  If replacement steel is tied, cut the existing steel to leave the lap length plus 50 millimeters.  Lap lengths are shown in Table 501-2.

Table 501-2

Reinforcing Steel Splices

| Bar Size | Length of Overlap (Millimeters) |
| --- | --- |
| 10M | 375 |
| 15M | 450 |
| 20M | 550 |

Remove the concrete by either or both of the following methods:

(1) Break-up and clean-out method.  Break up the concrete from the center of the patch area toward the end saw cuts.  Remove the concrete pieces with equipment that will not damage the underlying surface.

(2) Lift-out method.  Lift the slab in one or more pieces without disturbing the underlying surface.  Clean out the area with hand tools.

Dispose of the concrete according to Section 203.  When directed, excavate the underlying material to a maximum depth of 300 millimeters, and replace with aggregate base according to Sections 204 and 301.  Prevent adjacent concrete slabs from being undermined.

Remove and replace adjacent slabs damaged by concrete removal.  Repair spalls using partial-depth patching methods according to Section 502.

Repair all saw overcuts at the corner of repair areas and nicks to adjacent pavement outside the perimeter of the repair area with non-corrosive, non-shrink grout.

(b) Replacing reinforcing steel.  For continuously reinforced concrete pavement, if more than 10 percent of the reinforcing steel is visibly corroded or damaged, extend the limits of the patch over the required lap length.  The required lap lengths for various sizes of reinforcing steel bars are shown in Table 501-2.

For concrete pavement patches, provide a 75-millimeter clearance between the ends of new reinforcing steel and the existing slab face.  Match the number, type, and spacing of the new reinforcement to the existing pavement.  Support reinforcing steel with bar chairs or other approved methods while placing concrete.

(c) Joints.  Construct joints according to Subsection 501.08.  Field adjust locations and lengths of joints as directed at intersections, median openings, and other areas of odd-shaped slabs such that no joint is less than 460 millimeters long and no slab has an angle less than 60 degrees.  Construct joints perpendicular to the edge of pavement.

Place dowels or tie bars into the existing slab.  Drill the dowel or tie bar holes into the face at the required diameter with the drill rigidly supported.  Completely fill the holes around the dowels and tie bars with an epoxy or nonshrink grout for a permanent fastening to the existing concrete.  Furnish a plug or donut to prevent epoxy or grout loss.

Edge all transverse and longitudinal joints against forms or existing pavement.  Transverse joints in a continuous lane pour or longitudinal joints in a continuous dual lane pour do not require edging.

Clean the exposed faces of joints according to Subsection 502.06(a).  Seal joints according to Subsection 501.11.

(d) Concrete placement.  Construct side forms to overlap the ends of the existing slab.  Securely fasten side forms so they do not move when concrete is placed.  To accommodate forms for the patch, excavate the adjacent shoulders a maximum width of 300 millimeters.

Cast each patch in one continuous full-depth operation.  After removal of the forms, backfill, compact, and return the excavated shoulder area to its previous condition.

(e) Finishing.  Finish patches according to Subsection 501.09 to match the plane and texture of the contiguous pavement.

501.14  Opening to Traffic.  Do not allow traffic on new concrete pavement earlier than 14 days after concrete placement unless concrete tests indicate one of the following conditions is obtained:

(a) Flexural strength of 4 megapascals according to AASHTO T 97; or

(b) Compressive strength of 25 megapascals according to AASHTO T 22.

Cure specimens according to AASHTO T 23, Curing, Curing for Determining Form Removal Time or When a Structure May be Put into Service.

Do not allow traffic on the pavement when joint sealant is tacky and traffic debris would imbed into the sealant.

501.15  Acceptance.  Material (except reinforcing steel) for rigid pavement will be evaluated under Subsections 106.02 and 106.03.  Furnish a production certification for the hydraulic cement.

The concrete mixture's slump, air content, unit mass, and temperature will be evaluated under Subsections 106.02 and 106.04.  See Table 501-3 for sampling and testing requirements.

Type B pavement roughness will be evaluated under Subsection 106.04.  See Subsection 501.12.

Concrete compressive strength, pavement thickness, and type A pavement smoothness will be evaluated under Subsection 106.05.  See Table 501-3 for sampling and testing requirements.

(a) Compressive strength.  The lower specification limit is the minimum required compressive strength at 28 days (fc') specified in Table 501-1.  A single compressive strength test result is the average result from 2 cylinders cast from the same load and tested at 28 days.  See Table 501-3 for the acceptance quality characteristic category.

(b) Pavement thickness.  The lower specification limit is the required thickness minus 6 millimeters.  See Table 501-3 for the acceptance quality characteristic category.

(c)  Pavement smoothness.  The evaluation will be made after all defective areas are corrected.  See Subsection 501.12.

Construction (including batching, placing, finishing, and curing concrete) of the rigid pavement will be evaluated under Subsections 106.02 and 106.04.

Reinforcing steel will be evaluated under Section 554.

Measurement

501.16  Measure the Section 501 items listed in the bid schedule according to Subsection 109.02 and the following as applicable.

Measure the square meter width horizontally including allowable curve widening.  Measure the square meter length horizontally along the centerline of the roadway.

Measure sealing joints under Section 502.

Measure removal and disposal of unsuitable material in the subbase or subgrade under Section 204.

Measure patching and leveling material used to replace unsuitable material removed from the roadbed under the applicable Sections.

Payment

501.17  The accepted quantities will be paid at the contract price per unit of measurement for the Section 501 pay items listed in the bid schedule except the rigid pavement unit bid price will be adjusted according to Subsections 106.05 and 501.12.  Payment will be full compensation for the work prescribed in this Section.  See Subsection 109.05.

Payment for rigid pavement will be made at a price determined by multiplying the unit bid price by the material pay factor.  The material pay factor is the lowest single pay factor determined for either compressive strength or pavement thickness.

When the bid schedule contains a pay item for rigid pavement, type A pavement smoothness, a separate adjustment will be made for pavement smoothness according to the following formula:

A2 = 20,300(PFsmooth – 1.00)(L)

where:

A2	= Adjustment to contract payment in dollars for pavement smoothness.

L	=  Total project length in lane kilometers of traveled way including excluded areas.  Measure project length to 3 decimal places.

PFsmooth 	=  Pay factor for smoothness with respect to the upper specification limit of 380 millimeters per kilometer after completion of corrective work.

When the bid schedule contains a pay item for rigid pavement, type B pavement roughness, a separate pay adjustment will be made.  The dollar amount of the adjustment will be determined by summing the pay adjustment factors determined in Subsection 401.16 for each 0.1-kilometer and multiplying that sum by the contract unit bid price.

| Table 501-3 Sampling and Testing Requirements | Reporting Time | Before producing | Before producing | Before batching | “ | “ |
| --- | --- | --- | --- | --- | --- | --- |
|  | Split Sample | Yes | Yes | Yes, when requested | “ | “ |
|  | Point of Sampling | Source of material | Source of material | Flowing aggregate stream (bin, belt, discharge conveyor belt, or stockpile) | “ | “ |
|  | Sampling Frequency | 1 per material type | 1 per mix design | 1 per day | — | — |
|  | Test Methods Specifications | AASHTO M 80 | Subsection 552.03 | AASHTO T 27 & T 11 | AASHTO T 27 | AASHTO T 255 |
|  | Category | — | — | — | — | — |
|  | Characteristic | Quality | All | Gradation | Fineness modulus | Moisture test |
|  | Type of Acceptance (Subsection) | Measured and tested for conformance (106.04 & 105) | Measured and tested for conformance (106.04 & 105) | Measured and tested for conformance (106.04) |  |  |
|  | Material or Product | Aggregate source quality (703.02) | Concrete composition (mix design) | Produced aggregate (fine & coarse) |  |  |

| Table 501-3 (continued) Sampling and Testing Requirements | Reporting Time | Upon completing tests | “ | “ | “ | Subsection 552.09(b)(4) | Upon completing paving | “ | 72 hours | (1) Sample according to AASHTO T 141 except composite samples are not required. | (2) Cast at least 4 compressive strength test cylinders and carefully transports the cylinders to the job site curing facility. | (3) A single compressive strength test result is the average result from 2 cylinders cast from the same lead and tested at 28 days. | (4) Deliver cylinders to designated laboratory for test. | (5) Thickness is not a statistically evaluated parameter unless concrete pavement payment is by the square meter. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Split Sample | — | — | — | — | Note 4 | — | — | — |  |  |  |  |  |
|  | Point of Sampling | Point of discharge | “ | “ | “ | Discharge stream at point of placement | See Subsection 501.12 | See Subsection 501.12 | In place after sufficient hardening |  |  |  |  |  |
|  | Sampling Frequency | 1 per load | “ | “ | “ | 1 set per 25 m3 but not less than 1 per day | See Subsection 501.12 | See Subsection 501.12 | 1 core per 2000 m2 |  |  |  |  |  |
|  | Test Methods Specifications | AASHTO T 121 | AASHTO T 152 or T 196 | AASHTO T 119 | Field measured | AASHTO T 23 & T 22 | See Subsection 501.12 | See Subsection 501.12 | AASHTO T 24 |  |  |  |  |  |
|  | Category | — | — | — | — | II | I | — | II |  |  |  |  |  |
|  | Characteristic | Unit mass | Air content | Slump | Temperature | Compressive strength(2)(3) | Type A smoothness | Type B roughness | Pavement thickness (5) |  |  |  |  |  |
|  | Type of Acceptance (Subsection) | Measured and tested for conformance (106.04) |  |  |  | Statistical (106.05) | Statistical (106.05) | Measured and tested for conformance (106.04) | Statistical (106.05) |  |  |  |  |  |
|  | Material or Product | Concrete(1) (552.09 (b)(3)) |  |  |  | Structural concrete (552.09 (b)(3)) | Concrete pavement |  |  |  |  |  |  |  |

## Section 502. — RIGID PAVEMENT RESTORATION

Description

502.01  This work consists of the restoration of rigid pavement.  This work includes partial-depth patching, pavement jacking, subsealing, surface grinding, crack and joint repair, and breaking and seating before a pavement overlay.

Material

502.02  Conform to the following Section and Subsections:

Epoxy grout	725.22(b)

Epoxy resin adhesives	725.21

Joint fillers and sealants	712.01

Non-shrink grout	725.22(c)

Polymer grout	725.22(b)

Rigid pavement	501

Water	725.01

Construction Requirements

502.03  Composition of Mix (Concrete Mix Design).  Design the concrete mix according to Subsection 501.03.  Provide cement which is similar in color to that used in existing pavement.  Provide aggregates which are similar in gradation, color, and hardness to those used in existing pavement.

502.04  Equipment.  Furnish equipment conforming to Section 501 and the following:

(a) Rigid pavement removal.  Furnish removal equipment that will not fracture the concrete below the necessary patch depth.

(b) Routing.  Furnish routers that control and maintain the required cutting depth and width without damaging the adjacent concrete or remaining joint material.

(c) Sandblasting.  Furnish sandblasting equipment that will remove any residual sealant, oil, or other foreign material in joints that may prevent bond of new sealant.

(d) Jet waterblasting.  Furnish a high-pressure water jet machine that is capable of removing all residual sealant, oil, or other foreign material in joints that may prevent the new sealant from bonding.

(e) Air compressors.  Furnish air compressors with a minimum nozzle pressure of 690 kilopascals and capable of dislodging loose debris and drying joints and cracks.

(f) Joint and crack sealing.  Furnish sealing equipment according to the manufacturer's recommendations for the sealing material furnished.

(g) Grouting.  Furnish a grout plant which consists of a positive displacement cement injection pump and a high-speed colloidal mill.  Operate colloidal mixing machine at speeds necessary to make a homogeneous mixture.

Furnish an injection pump having a pressure capability of 1900±170 kilopascals when pumping a grout slurry mixed to a 12-second flow cone time and that continuously pumps at a minimum rate of 6.0 liters per minute.  The system may be modified by adding a recirculating hose and valve at the discharge end of the pump.

Batch water through a meter or scale capable of measuring the total day's consumption.  Furnish hoses, fittings, and control which provide a positive seal during grout injection.

(h) Drilling.  Furnish rock drills capable of drilling straight and true minimum 38-millimeter holes through the concrete slab, steel reinforcement, and base material.

Furnish rock drills weighing less than 27 kilograms that are capable of drilling with a downward pressure of less than 90 kilograms.  Furnish an auger to open clogged holes and existing pavement jacking holes.

(i) Slab stabilization testing.  Furnish testing equipment including the following:

(1) A 2-axle truck with dual rear wheels.  Load the rear axle to 80 kilonewtons evenly distributed between the 2 wheel paths;

(2) Static load measuring gauges consisting of 4 gauges on 2 gauge mounts, 2 gauges per mount, capable of detecting slab movement under load; and

(3) A modified Benkelman beam or similar approved device.

(j) Surface diamond grinding.  Furnish power driven, self-propelled grinding equipment, specifically designed to smooth and texture concrete pavement with diamond blades.  Furnish equipment that:

(1) Cuts or planes at least 1 meter in width;

(2) Does not encroach on traffic movement outside of the work area; and

(3) Grinds the surface without spalling at joints and cracks or fracturing surface aggregates.

(k) Fracturing and seating.  Furnish an approved fracturing device capable of producing the desired fracturing pattern without displacing or spalling the pavement.  "Headache balls" and vibratory pneumatic hammers will not be permitted.

Furnish at least a 32-metric ton pneumatic tired roller to seat the broken pavement.  Towing equipment shall have pneumatic tires and shall move the roller forward and backward along predetermined lines.

502.05  Partial-Depth Patching.  This work consists of patching spalls, potholes, corner breaks, or other surface distresses in concrete pavement.

Construct the pavement patch similar in appearance to the existing pavement.  Prepare test panels using the same material proposed for the work.  Begin concrete pavement work after approval of the concrete mix design and the test panel appearance.

(a) Patch material.  Use an epoxy grout or polymer concrete patch material for patches less than or equal to 40 millimeters deep.  Use hydraulic cement concrete for patches greater than 40 millimeters deep.

(b) Patch area preparation.  Extend the limits of repair areas a minimum of 100 millimeters outside the area of delamination.  Saw cut the perimeter of the patch area, parallel to the existing joint, to a minimum depth of 40 millimeters and provide a vertical face at the edge of the patch.  Near vertical edges from milling or grinding machines are acceptable.  Repair all saw overcuts at corners of repair areas and nicks to adjacent pavement outside the perimeter of the repair area with noncorrosive, nonshrink grout.

Break out concrete within the patch area to a minimum depth of 40 millimeters to expose sound and clean concrete.  If the depth of the repair exceeds 100 millimeters, remove and replace the repair area as a full-width, full-depth slab according to Subsection 501.13.

Sandblast exposed concrete faces clean of loose particles, oil, dust, traces of asphalt concrete, and other contaminants before patching.  Remove sandblasting residue immediately before placing the epoxy resin adhesive.

Remove shoulders adjacent to the patch longitudinally to the depth of the patch and to a maximum width of 300 millimeters to facilitate placing form work.  Patch and compact shoulders with material similar to the existing shoulder.  Dispose of the concrete according to Section 203.05.

(c) Placing patch material.  Apply an epoxy resin adhesive according to the manufacturer's recommendations.  Delay concrete placement until the epoxy becomes tacky.  Place and consolidate the patch mixture to eliminate voids at the interface of the patch and existing concrete.  Finish patches according to Subsection 501.09 to match the plane and texture of the contiguous pavement.  Cure according to Subsection 501.10.

(d) Joints.  If a partial-depth repair area abuts a working joint, repair the joint similar to the existing joint to maintain a working joint.  Form a new joint to the same width as the existing joint.  Seal the joint according to Subsection 502.06.

502.06  Joint and Crack Repair.  This work consists of repairing and resealing joints and cracks in existing concrete pavement.

(a) Preparation of joints and cracks.  Clean and reseal longitudinal and transverse joints as required.  Remove the existing material in the joints, and clean the joint no earlier than 1 day before resealing.  Do not damage joints or previously-repaired patches.

Remove sealant with a router to a minimum depth of 2.5 times the joint width to accommodate the backer rod and to provide the required depth for the new sealant.  After routing, clean the adjacent pavement surfaces.

Reface cracks with a concrete saw.  Remove old sealant from the crack faces to expose new, clean concrete.  When the crack widths vary and the crack faces are ravelled and irregular, cut a crack reservoir depth of 20 millimeters.

Thoroughly clean the joint or crack of all foreign material.  Clean the joint by sandblasting, high-pressure water jet, or with a mechanical wire brush.  Repeat the process until a new, clean concrete face is exposed.  Dry the joint with compressed air.

Use sawing if other methods do not properly clean the joint.  Limit sawing to exposing clean, new, concrete faces in the joint with a minimum allowable cut of 2 millimeters on each face of the joint.

(b) Backer rod.  Install the backer rod to the required depth after the joints and cracks are clean and dry.  Do not stretch or twist the backer rod during installation.  Limit the length of backer rod installed to that which can be sealed during the same workday.

(c) Sealant application.  Seal joints and cracks immediately after placing the backer rod.  Apply sealant at the air and surface temperatures recommended by the sealant manufacturer.  If the joint or crack becomes contaminated or damp, remove the backer rod, clean and dry the joint or crack, and reinstall a new backer rod before placing the sealant.  Immediately after application, tool the sealant to provide firm contact with the joint faces and to form the required recess below the slab surface.

502.07  Pavement Jacking.  This work consists of raising and supporting the concrete pavement to the specified grade tolerances by drilling and injecting non-shrink hydraulic cement grout.

(a) Drilling holes.  Determine a pattern for grout injection holes and submit for approval.  Drill holes vertically, round, and less than 50 millimeters in diameter.  Prevent breaking out the bottom of the pavement.

(b) Jacking.  Establish string lines from the pavement high points to monitor slab movement.  Lower an expanding rubber packer or hose, providing a positive seal and connected to the discharge hose on the grout plant, into the holes.  Do not allow the discharge end of the packer or hose to extend below the lower surface of the concrete pavement.

When jacking continuously-reinforced concrete pavement, allow pumping to raise the pavement to within 3 millimeters of the string line grade.  When jacking jointed pavement and bridge approach slabs, allow pumping to raise the pavement to within 6 millimeters of the transverse and longitudinal grades.

Continuous pressures to 1.4 megapascals are permitted.  Use pressures to 2 megapascals only for short periods (30 seconds or less).  If the pavement is bonded to the subbase, brief pressure rises (10 seconds or less) to 4.1 megapascals may be allowed.  Stop pumping if grout extrudes through cracks, joints, shoulders, or from back pressure in the hose.

(c) Overjacking.  Grind pavement raised above the specified tolerances to grade.  If the overjacking is greater than 25 millimeters, remove and replace the pavement or a portion thereof, according to Subsection 501.13.

(d) Cracks.  New cracks radiating through the grout injection holes are presumed to have been caused by improper injection techniques.  If any cracks emanate from any grout injection hole, remove and replace the slab or a portion of the slab according to Subsection 501.13.

(e) Hole patching.  After the grout has set and the hole plugs are removed, remove all grout from the holes for the full depth of the slab, and fill the holes with an epoxy mortar.  Repair damaged holes.

502.08  Undersealing and Slab Stabilization.  This work consists of pumping a non-shrink hydraulic cement grout mixture through holes drilled in the pavement into voids underneath the slabs to stabilize and underseal concrete pavement.

(a) Preliminary testing.  Perform all testing at night or when there is no evidence of slab lock-up due to thermal expansion.  Testing may be allowed to continue if the slabs are not interlocked or under compression.  Furnish testing equipment as provided in Subsection 502.04(i).

Test each designated slab using a static method as follows:

(1) Position one set of gauges with one gauge referenced to the corner of each slab on both sides of the joint near the pavement edge.

(2) Set the gauges to zero with no load on the slab on either side of the joint.

(3) Move the test truck into position and stop with the center of the test axle 300 millimeters behind the joint and the outside test wheel 300 millimeters from the pavement edge.  Read the back gauge.

(4) Move the test truck across the joint to a similar position 300 millimeters forward from the joint and stop.  Read the forward gauge.

(5) Repeat for each joint to be tested.  Underseal all slabs with a deflection of more than 0.8 millimeter.

(b) Drilling Holes.  Drill holes using the required hole pattern.  An altered hole pattern may be approved based on slab testing and field conditions.  Size drilled holes to provide a positive seal for the pumping nozzle.  For the first undersealing, drill holes to a depth of 75 millimeters beneath the bottom of the concrete.

Submit the number, depth, and location of holes for the second undersealing for review and approval.

(c) Cleaning holes.  After the holes are drilled and before pumping the underseal grout, clean the hole with compressed air to remove debris and provide a passage for the grout.

(d) Pumping underseal grout.  Pump grout in all holes.  Seal the nozzle of the discharge hose in the hole to maintain the grout pressure underneath the slab.  Do not allow the nozzle end to extend below the bottom of the concrete.

Continue pumping into a hole until grout flows out other holes, joints, or cracks, or until the slab begins to lift.  Stop grouting if there is any lift in the slab or the adjacent shoulder.

During pumping and grouting, closely monitor lift measuring devices to prevent pumping pressures greater than 700 kilopascals and slab lift greater than 1.3 millimeters total accumulative movement measured at the outside joint corner.  Do not plug holes while grouting.

Prevent the slab from cracking or breaking.  Remove and replace damaged slabs according to Subsection 501.13.

(e) Permanently sealing holes.  After the grout has set, remove all grout from the holes for the full depth of the slab and fill the holes with a non-shrink grout or epoxy mortar.  Repair damaged holes.

(f) Stability testing.  After the designated slabs have been undersealed and tested according to (a) above and after 24 hours have elapsed, underseal any slab that continues to show excess movement.  The CO may accept or direct replacement of any slab that continues to show movement in excess of that specified after undersealing twice.  Remove and replace designated slabs according to Subsection 501.13.

502.09  Surface Diamond Grinding.  This work consists of grinding existing concrete pavement to eliminate joint or crack faults and providing positive lateral drainage.  Uniformly transition auxiliary or ramp lane grinding from the mainline edge to provide positive drainage and an acceptable riding surface.

Remove solid residue from pavement surfaces before it is blown by traffic or wind.  Do not allow residue to flow across lanes used by public traffic or into drainage facilities.

Produce a surface texture consisting of parallel grooves 3±0.5 millimeters wide.  Provide an area between the grooves 2.2±0.5 millimeters, and a difference between the peaks of the ridges and the bottom of the grooves of approximately 2 millimeters.

Test the ground pavement surfaces for pavement smoothness according to Subsection 501.12(b).  Check transverse joints and random cracks with a 3-meter straightedge.  Misalignment of surface planes on adjacent sides of the joints or cracks and between each grinding pass shall be less than 1.6 millimeters.  The transverse slope of the pavement shall have no depressions or slope misalignment greater than 6 millimeters in 3 meters tested perpendicular to the centerline.  Straightedge requirements do not apply across longitudinal joints or outside of ground areas.

502.10  Fracturing Concrete Pavement.  This work consists of fracturing existing concrete pavement and firmly seating or compacting the pavement before a pavement overlay.  Use one of the following methods:

(a) Crack and seat.  Crack the existing concrete pavement into full-depth hairline cracks with pieces approximately 0.5 to 1.0 meters in size.  Seat the pieces firmly into the foundation.

(b) Break and seat.  Break the existing concrete pavement into full-depth hairline cracks with pieces approximately 0.4 to 0.6 meters in size.  Rupture the reinforcement or break the concrete bond and seat the pieces firmly into the foundation.

(c) Rubblize and compact.  Completely fracture the existing pavement into pieces approximately 0.05 to 0.15 meters in size.  Remove exposed reinforcing steel and wire mesh.  Compact the pieces into a layer.

The CO will designate a test section.  Fracture the test section using varying energy and striking heights to establish a satisfactory, evenly-distributed crack pattern.  Obtain 150-millimeter diameter pavement cores at 10 designated locations over the cracks to verify that the cracks are full depth.

When fracturing a test section, furnish and apply water to dampen the pavement following fracturing to enhance visual determination of the fracturing pattern.  Furnish and apply water to a checked section at least once a day to verify that a satisfactory fracture pattern is maintained.  If approved, adjust the energy and striking height based on check sections.

Seating consists of rolling the rigid pavement, 2 passes minimum with a 45-metric ton roller or 4 to 7 passes with a 32-metric ton roller, until the concrete pieces are firmly seated.  Compacting consists of rolling the rigid pavement, 2 passes minimum with a 9-metric ton vibratory roller.  The CO will determine the maximum number of roller passes on the test section to ensure seating or compacting without damaging the pavement.  Remove all loose pieces of broken concrete that are not firmly seated.

Tack the near vertical sides where full-depth broken concrete is removed according to Section 412.  Fill the hole with asphalt concrete according to Section 404.

Prevent the formation of continuous longitudinal cracks.  Do not fracture pavement within 3 meters of existing box or pipe culverts.

Fill 25-millimeter or greater depressions, resulting from the compaction, with graded aggregate and recompact.

If unable to fracture pavement to the specified size due to poor subgrade, remove the pavement and replace with aggregate according to Section 301.

Clean and seal existing joints and cracks greater than 13 millimeters width according to Subsection 414.05.

Place the first course of asphalt concrete within 48 hours following the fracturing operation.  If the pavement is used to maintain traffic after fracturing, but before the asphalt concrete overlay, sweep and patch to maintain a safe riding surface.

502.11  Opening to Traffic.  Do not allow traffic on patched pavement until the concrete has a compressive strength of 25 megapascals when tested according to AASHTO T 22 or until the grout used for jacking or undersealing the pavement has attained 4.2 megapascals when tested with a 160-square millimeter probe according to AASHTO T 197.

Do not allow traffic on sealed joints when the sealant is tacky and traffic debris embeds into the sealant.

502.12  Acceptance.  See Table 502-1 for sampling and testing requirements.

Material for rigid concrete pavement restoration will be evaluated under Subsections 106.02 and 106.03.  Furnish a production certification for the hydraulic cement.

The concrete mixture's slump, air content, unit mass, and temperature will be evaluated under Subsections 106.02 and 106.04.

The concrete compressive strength will be evaluated under Subsection 106.04.  The lower specification limit is the minimum required compressive strength at 28 days (fc') specified in Table 501-1.  A single compressive strength test result is the average result from two cylinders cast from the same load and tested at 28 days.

Construction (including batching, placing, finishing, and curing concrete) of the concrete will be evaluated under Subsections 106.02 and 106.04.

Grout will be evaluated under Subsections 106.02 and 106.03.

Rigid pavement restoration work (including partial-depth patching, pavement jacking, subsealing, surface grinding, crack and joint repair, and breaking and seating) will be evaluated under Subsections 106.02 and 106.04.

Measurement

502.13  Measure the Section 502 items listed in the bid schedule according to Subsection 109.02 and the following as applicable.

Measure grout for pavement jacking and undersealing by the cubic meter by metering.

Measure full-depth, full-width pavement patches under Section 501.

Measure slabs ordered replaced after undersealing twice under Section 501.

Measure aggregate base under Section 301.

Payment

502.14  The accepted quantities will be paid at the contract price per unit of measurement for the Section 502 pay items listed in the bid schedule.  Payment will be full compensation for the work prescribed in this Section.  See Subsection 109.05

| Table 502-1 Sampling and Testing Requirements | Reporting Time | Before producing | Before producing | Before batching | “ | “ |
| --- | --- | --- | --- | --- | --- | --- |
|  | Split Sample | Yes | Yes | Yes, when requested | “ | “ |
|  | Point of Sampling | Source of material | Source of material | Flowing aggregate stream (bin, belt, discharge conveyor belt, or stockpile) | “ | “ |
|  | Sampling Frequency | 1 per material type | 1 per mix design | 1 per day | — | — |
|  | Test Methods Specifications | AASHTO M 80 | Subsection 552.03 | AASHTO T 27 & T 11 | AASHTO T 27 | AASHTO T 255 |
|  | Category | — | — | — | — | — |
|  | Characteristic | Quality | All | Gradation | Fineness modulus | Moisture test |
|  | Type of Acceptance (Subsection) | Measured and tested for conformance (106.04 & 105) | Measured and tested for conformance (106.04 & 105) | Measured and tested for conformance (106.04) |  |  |
|  | Material or Product | Aggregate source quality (703.02) | Concrete composition | Produced aggregate (fine & coarse) |  |  |

| Table 502-1 (continued) Sampling Testing Requirements | Reporting Time | Upon completing tests | “ | “ | “ | See 552.09(b)(4) | (1) Sample according to AASHTO T 141 except composite samples are not required. | (2) Cast at least 4 compressive strength test cylinders and carefully transport the cylinders to the job site curing facility. | (3) A single compressive strength test result is the average result from 2 cylinders cast from the same lead and tested at 28 days. | (4) Deliver cylinders to designated laboratory for test. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Split Sample | — | — | — | — | Note 4 |  |  |  |  |
|  | Point of Sampling | Point of discharge (1) | “ | “ | “ | Discharge stream at point of placing |  |  |  |  |
|  | Sampling Frequency | 1 per load (2) | “ | “ | “ | 1 set per 25 m3 but not less than 1 per day |  |  |  |  |
|  | Test Methods Specifications | AASHTO T 121 | AASHTO T 152 or T 196 | AASHTO T 119 | Field measured | AASHTO T 23 & T 22 |  |  |  |  |
|  | Category | — | — | — | — | II |  |  |  |  |
|  | Characteristic | Unit mass | Air content | Slump | Temperature | Compressive strength(3) |  |  |  |  |
|  | Type of Acceptance (Subsection) | Measured and tested for conformance (106.04) |  |  |  | Statistical (106.05) |  |  |  |  |
|  | Material or Product | Concrete (552.09(b)(3)) |  |  |  | Structural concrete (552.09(b)(3)) |  |  |  |  |