03USC09/14/08

Section 608. — PAVED WATERWAYS

| Include the following when work is required under this Section. Edit as required. | (WFL Specification 09/14/08) |
| --- | --- |

Delete the text of Table 608-1 and substitute the following:

| Table 608-1 Sampling and Testing Requirements | Reporting Time | 24 hours | " | " | " | (1) Sample consists of 2 test specimens. (2) The compressive strength will be the average of two test specimens. |
| --- | --- | --- | --- | --- | --- | --- |
|  | Split Sample | Yes, when requested | " | " | " |  |
|  | Point of Sampling | Production output or stockpile | " | " | Job site |  |
|  | Sampling Frequency | 1 per 600 yd3 | " | " | 1 per installation (1) |  |
|  | Test Methods Specifications | AASHTO T 27 & T 11 | AASHTO T 89, Method A & T 87 | AASHTO T 27 & T 11 | AASHTO T 23 & T 22 |  |
|  | Category | — | — | — | — |  |
|  | Characteristic | Gradation | Liquid limit | Gradation | Making test specimens Compressive strength (2) |  |
|  | Type of Acceptance (Subsection) | Measured and tested for conformance (106.04) |  | " | " |  |
|  | Material or Product | Bed course |  | Granular backfill | Mortar |  |